Supporting Information

Ultrathin MoO2 Nanosheets Encapsulated in Carbon Matrix for Superior Lithium Storage

Jiangfeng Nia, Yang Zhaoa, Liang Lia, *, Liqiang Maib, *

a College of Physics, Optoelectronics and Energy & Collaborative Innovation Center of Suzhou Nano Science and Technology, Soochow University, Suzhou 215006, China

b State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, WUT-Harvard Joint Nano Key Laboratory, Wuhan University of Technology, Wuhan 430070, China

* Corresponding authors. Tel: +86-87467595, Fax: +86-27-87644867

E-mail addresses: lli@suda.edu.cn (L. Li), mlq518@whut.edu.cn (L. Mai)

Table S1 Li storage capability of the MoO2/C nanosheets in comparison with other MoO2 nanomaterials.

| MoO2 Sample | a Retention / Cycle | Rate capability | Reference |
| --- | --- | --- | --- |
| Mesporous MoO2 | 670 mAh g−1 / 30 cycles | 450 mAh g−1 at 0.08 A g−1 | [11] |
| MoO2/C nanosphere | 570 mAh g−1 / 30 cycles | b410 mAh g−1 at 3 C | [12] |
| MoO2/C nanowire | 467 mAh g−1 / 30 cycles | 356 mAh g−1 at 1.0 A g−1- | [7] |
| MoO2/C nanocrystal | 554 mAh g−1 / 70 cycles | 575 mAh g−1 at 0.4 A g−1 | [5] |
| MoO2/rGO | 598 mAh g−1 / 70 cycles | 408 mAh g−1 at 2 A g−1 | [14] |
| MoO2 nanorod | 830 mAh g−1 / 30 cycles | 80 mAh g−1 at 0.8A g−1 | [9] |
| MoO2/rGO | 640 mAh g−1 / 50 cycles | 380mAh g−1 at 2 A g−1 | [18] |
| MoO2/C nanobelt | 617 mAh g−1 / 30 cycles | 434 mAh g−1 at 1 A g−1 | [10] |
| MoO2/OMC | 668 mAh g−1 / 50 cycles | 401 mAh g−1 at 2 A g−1 | [13] |
| Amorphous MoO2 | 800 mAh g−1 / 50 cycles | c705 mAh g−1 at 5 A g−1 | [20] |
| MoO3/C | d 521 mAh g−1 / 300 cycles | 483 mAh g−1 at 3 A g−1 | [35] |
| MoS2/CNT | 698 mAh g−1 / 60 cycles | 369 mAh g−1 at 1 A g−1 | [36] |
| FeS/C nanosheet | 615 mAh g−1 / 100 cycles | 349 mAh g−1 at 3 A g−1 | [37] |
| MoO2/C nanosheet | 1051 mAh g−1 / 100 cycles | 719 mAh g−1 at 5 A g−1 | This work |

a The current rate for this work is 0.5 A g−1, while it is no greater than 0.5 A g−1 for others;

b The exact value for C is unknown;

c The lithiation (discharge) is restricted to a much lower rate of 0.1 A g−1.

d The capacity was calculated based on the total mass of MoO3 and C as it does in our work.

Figure S1 TEM images of hydrothermally prepared MoO3 samples for various reaction times (a) 3 h, (b) 6 h, (c) 12 h, and (d) 24 h. The images show that MoO3 nanosheets are formed and developed when the reaction time extends to 12 h and beyond.

Figure S2 TEM image of MoO2/C showing sheet-like morphology.

Figure S3 EDS of MoO2/C product. The diagram confirms that the product is composed of elements Mo, O, and C.

Figure S4 TG-DTA curves of MoO2/C nanosheets in flowing air. The mass gain before 250 °C can be ascribed to MoO2 oxidation to MoO3, while the mass loss between 300 to 400 °C is due to burning out of amorphous carbon.

Figure S5 (a) Cyclic voltammograms and (b) charge and discharge profiles of MoO2 nanosheet electrodes during initial cycles. The drastic variation in the CV and discharge curves during initial cycles suggests a poor reversibility for the pure MoO2 nanosheets. The initial discharge and charge capacity are 1387.5 and 972.4 mAh g−1, resulting in a CE of ~70% compared to 78% of carbon encapsulated counterpart.

Figure S6 Impedance spectra of MoO2/C nanosheet electrodes before cycle and after 100 cycles at 0.5 A g−1. The spectra were collected at charged state in the frequency range of 0.1–100k Hz using an AC signal of 5 mV. No apparent change is observed in the semicircles at high and middle frequencies, suggesting that neither Li diffusion across passivation film nor subsequent charge transfer process is interfered. Meanwhile, the reduced length of spike line in the low frequency indicates improved diffusion capability of Li within the electrode.

Figure S7 Post TEM image of MoO2/C nanosheet after 100 cycles at 0.5 A g−1. Surface amorphous layer out of the crystalline core is clearly visible. The interplanar spacing of 0.24 nm corresponds to (200) plane of monoclinic MoO2 crystal.

Figure S8 Charge and discharge curves of MoO2/C nanosheet electrodes at varying current rates. The profiles are primarily preserved when the current rate increases from 0.25 to 10 A g−1.

Figure S9 Charge and discharge curves of MoO3 nanosheet electrodes at varying current rates.

Figure S10 (a) Discahrge curve and (b) EIS spectrum of the MoO2/C nanosheet electrode. The electrode was discharged to 1.2 V and then held at this potential for 6 h before impedance test. The phase >45 ° at low frequency region indicates a capacitive behavior of the MoO2/C electrode.