Supporting information

Graphene Wrapped NASICON-type Fe2(MoO4)3 Nanoparticles as a Ultra-high Rate Cathode for Sodium Ion Batteries

Jinzhi Shenga,1, Han Zanga,1, Chunjuan Tanga,b,1, Qinyou Ana,*, Qiulong Weia, Guobin Zhanga, Lineng Chena, Chen Penga and Liqiang Maia,*

Figure S1 SEM images of the precursor under stiring after 10 min (a), 30 min (b) and 60 min (c).

Figure S2 XRD pattern (a) and SEM images (b) of the precursor.

Figure S3 SEM images of pure graphene.

Figure S4 Nitrogen adsorption-desorption isotherms of FMO-H (a), FMO-M (b), FMO-MG (c) and the corresponding pore size distribution (insets).

Figure S5 EDS-mapping of FMO-MG after discharged to 1.5 V.

Figure S6 SEM images of electrode slices made by FMO-H (a), FMO-M (b), FMO-MG (c) before cycling; and electrode slices made by FMO-H (d), FMO-M (e), FMO-MG (f) after 20 cycles.

Figure S7 Charge-discharge curves of FMO-MG in different cycles.

Figure S8 (a) Cyclic voltammogram curves of FMO-MG at different scan rates; (b) CV curve for FMO-MG at a scan rate of 1 mV s-1, the estimated diffusion controlled capacity contribution is shown in the shaded region; (c) capacity contributions of FMO-MG under different scan rates.

Figure S9 Rate performance (a) and cycling performance (b) of the electrode prepared by mixing the active materials, acetylene black and PTFE in a weight ratio of 8:1:1.

Figure S10 SEM images of FMO-CNTs.

Figure S11 Rate performance (a) and cycling performance (b) of FMO-CNTs.

Equation S1

C ---- Specific capacity;

n ---- Transfer electronic number in a molecular;

F ---- Faraday constant;

M ---- The molecular weight

Table S1. Comparison of the Fe2(MoO4)3 SIB electrodes in the references.

| FMO samples | Voltage window | Specific capacity | Rate capacity | Electrode composition |
| --- | --- | --- | --- | --- |
| Fe2(MoO4)3 thin film[19] | 1.5-4.0 V | 94 mAh g-1 at 1 C | / | / |
| Pure Fe2(MoO4)3[20] | 2.5-3.1 V | 89.5 mAh g-1 at C/20 | / | Active material: carbon black: PVDF=8:1:1 |
| Fe2(MoO4)3/nanosilver composite[21] | 1.8-3.2 V | 92 mAh g-1 at 0.1 C | / | Active material: acetylene black: PTFE=80:15:5 |
| Fe2(MoO4)3/carbon nanotubes nanocomposite[22] | 1.5-3.5 V | 91 mAh g-1 at 0.1 C | 85 mAh g-1 at 1 C | Active material: acetylene black: PTFE=80:15:5 |
| Fe2(MoO4)3/RGO Nanocomposite[23] | 1.8-3.5 V | 90.6 mAh g-1 at 0.1 C | 80 mAh g-1 at 1.5 C | Active material: acetylene black: PTFE=80:15:5 |
| This work | 1.5-4.0 V | 98.4 mAh g-1 at 2 C | 64.1 mAh g-1 at 100 C | Active material: acetylene black: PTFE=6:3:1 |
| This work | 1.5-4.0 V | 90.7 mAh g-1 at 10 C | 60.9 mAh g-1 at 100 C | Active material: acetylene black: PTFE=8:1:1 |

Table S2. Resistances fitted by the EIS results.

|  | FMO-H | FMO-M | FMO-MG |
| --- | --- | --- | --- |
| Rs (Ω) | 7.3 | 6.2 | 5.1 |
| Rct (Ω) | 850 | 770 | 45 |