Supporting Information

Realizing stable lithium and sodium storage with high areal capacity using novel nanosheet-assembled compact CaV4O9 microflowers

Xiaoming Xu, Peijie Wu, Qi Li*, Wei Yang, Xiao Zhang, Xuanpeng Wang, Jiashen Meng, Chaojiang Niu, and Liqiang Mai*

State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, International School of Materials Science and Engineering, Wuhan University of Technology, Wuhan 430070, China

Fig. S1. Illustration of the synthesis procedure of nanosheet-assembled compact CaV4O9 microflowers.

Fig. S2. Crystal structures of CaV4O9 or SrV4O9. The green balls represent Ca or Sr ions, the red balls represent O ions, and the grey polyhedrals represent the V–O pyramids. (CaV4O9 and SrV4O9 are isostructural )

Table S1. Comparison of the crystallographic parameters between CaV4O9 and SrV4O9

|  | CaV4O9 | SrV4O9 |
| --- | --- | --- |
| JCPDS | 01-070-4469 | 01-070-4468 |
| Crystal system | Tetragonal | Tetragonal |
| Space group | P4/n | P4/n |
| a (Å) | 8.327 | 8.379 |
| b (Å) | 8.327 | 8.379 |
| c (Å) | 5.013 | 5.259 |

Fig. S3. (a) XRD pattern and (b) SEM image of CaV4O9 nanowires.

Fig. S4. The comparison of volume between CaV4O9 nanowires and the compact CaV4O9 microflowers in the case of same mass.

Fig. S5. TEM and HRTEM images of SrV4O9 microflower.

Fig. S6. Nitrogen adsorption-desorption isotherms and pore size distribution of CaV4O9 microflowers (a, b) and SrV4O9 microflowers (c, d).

Fig. S7. TG/DSC curves of unsintered CaV4O9 microflowers at Ar.

Fig. S8. TEM images of the CaV4O9 microflowers before calcination.

Fig. S9. SEM images of the Ca-V-O samples obtained at different hydrothermal time. (a,b) 1.0 h, (c,d) 1.5 h, (e,f) 2.0 h, (g,h) 3.0 h, (i,j) 6.0 h, (k,l) 48 h.

Fig. S10. The long-term cycling performance of CaV4O9 microflower for Li storage at current density of 1.0 A g-1 with a mass loading of 2.15 mg cm-2.

Table S2. Comparison of the mass loading, areal capacity and cycle life between compact CaV4O9 microflowers in this work and other reported LIB anodes with high areal capacity

| Materials | Mass loading (mg cm-2) | Stable areal capacity (mAh cm-2) | Current density (mA cm-2) | Cycle life | Reference |
| --- | --- | --- | --- | --- | --- |
| CaV4O9 microflowers | 4.4 | ~2.5 | 0.1 | 40 | This work |
|  | 3.42 | ~1.56 | 1.71 | 400 |  |
| SnO2/α-Fe2O3 nanotube array | – | ~0.9 | 0.1 | 50 | Nanoscale 4 (2012) 2760-2765 |
| Mesoporous Co3O4 nanosheet networks | 4.15 | 4.39 | 0.74 | 30 | Nano Energy 5 (2014) 91-96 |
| Mesoporous Si sponge | ~2.0 | ~1.5 | 0.75 | 300 | Nat. Commun. 5 (2014) 4105 |
| Multilayer Si/CNT coaxial nanofiber | – | 1.25 | – | 50 | Energy Environ. Sci. 7 (2014) 655-661 |
| Amorphous Si film | – | 0.6 | 0.225 | 200 | J. Power Sources 267 (2014) 629-634 |
| Graphene/Si–C composite | 3.2 | 3.2 | – | 100 | Nano Energy 6 (2014) 211-218 |
| Nanostructured Si secondary clusters | 2.02 | 2.3 | 0.5 | 100 | Energy Environ. Sci. 8 (2015) 2371-2376 |
| Pomegranate-like Si/C microspheres | 3.12 | 3.67 | 0.7 | 100 | Nat. Nanotechnol. 9 (2014) 187-192 |
| Graphene-encapsulated micrometer-sized Si particles | ~2.0 | ~2.2 | 1.4 | 120 | Nat. Energy 1 (2016) 15029 |
| Cu/Si/Ge nanowire arrays | 1.2 | ~1.5 | 0.48 | 100 | Energy Environ. Sci. 11 (2018) 669-681 |

Fig. S11. The CV curves of CaV4O9 microflower for Li storage (a) and Na storage (b) at a scan rate of 0.1 mV s-1.

Table S3. Comparison of the areal capacity between CaV4O9 microflower in this work and other reported SIB anodes using typical coating method

| Materials | Specific capacity (mAh g-1) | Mass loading (mg cm-2) | Current density (mA g-1) | Areal capacity (mAh cm-2) | Reference |
| --- | --- | --- | --- | --- | --- |
| CaV4O9 microflowers | ~ 275 | 3.65 | 100 | ~ 1.0 | This work |
| Expanded graphite | ~ 300 | ~ 0.5 | 20 | ~ 0.15 | Nat. Commun. 5 (2014) 4033 |
| Hard carbon | ~ 300 | 2.0 ~ 3.0 | 30 | 0.6 ~ 0.9 | J. Mater. Chem. A 4 (2016) 13046-13052 |
| Petal-like TiO2 | ~ 245 | ~ 1.2 | 83.75 | ~ 0.29 | Adv. Mater. 28 (2016) 9391-9399 |
| Na2Ti3O7@C hollow spheres | ~ 220 | ~ 1.0 | 177 | ~ 0.22 | Adv. Mater. 29 (2017) 1700989 |
| MoS2 nanosheets | ~ 575 | ~ 1.0 | 100 | ~ 0.57 | Adv. Energy Mater. (2017) 1702254 |
| Amorphous Sn2P2O7/rGO nanocomposite | ~ 480 | ~ 0.8 | 50 | ~ 0.38 | Adv. Energy Mater. (2017) 1701827 |
| FeS2/CNT network | ~ 530 | 0.5 ~ 1.0 | 200 | 0.26 ~ 0.53 | Nano Energy 46 (2018) 117-127 |
| TiO2/C | ~ 277 | ~ 1.5 | 50 | ~ 0.42 | Nano Energy 44 (2018) 217-227 |

Fig. S12. Characterization and electrochemical performance of Na3V2(PO4)3/C nanoparticles. (a) XRD pattern and (b) SEM image of Na3V2(PO4)3/C nanoparticles. (c) Charge-discharge profiles and (d) cycling performance of Na3V2(PO4)3/C nanoparticles at current rate of 1 C.

Fig. S13. Electrochemical performance of Na3V2(PO4)3//CaV4O9 Na-ion full battery. (a) Typical charge-discharge profiles of Na3V2(PO4)3 and CaV4O9. (b) Charge-discharge curves of the full cell at the voltage range from 0.5 to 3.2 V. (c) Illustration of the Na3V2(PO4)3//CaV4O9 all-vanadium Na-ion full battery. (d) Cycling performance of the full cell at a current density of 1.0 A g-1 (based on the mass of CaV4O9 microflowers).

Figure S14. SEM images of CaV4O9 microflowers after 500 cycles for Li storage at the current density of 1.0 A g-1.