Supporting Information

General and Precise Carbon Confinement of Functional Nanostructures Derived from Assembled Metal-Phenolic Network for Enhanced Lithium Storage

Zhitong Xiao, Jiashen Meng, Qi Li* Xiao Zhang, Ziang Liu, Bo Wen, Chunhua Han and Liqiang Mai*

State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, International School of Materials Science and Engineering, Wuhan University of Technology, Luoshi Road 122, Wuhan, 430070, Hubei, China.

*E-mail: qi.li@whut.edu.cn; mlq518@whut.edu.cn

Fig. S1 (a-f) TG curves of SnO2@C-Fe2O3-1, SnO2@C-Fe2O3-3, SnO2@C-Fe2O3-7, SnO2@C-Fe2O3-10, SnO2@C-Fe2O3-15 and SnO2@C-Fe2O3-20, respectively, in air at 10 °C min-1.

Fig. S2 The relationship between the content of Fe2O3 and the number of assembly layer according to the ICP results.

Fig. S3 (a, b) HRTEM images of SnO2@C-Fe2O3-1 and SnO2@C-Fe2O3-20, respectively.

Fig. S4 (a) XRD patterns of SnO2, SnO2@MPN-1, SnO2@MPN-3, SnO2@MPN-7, SnO2@MPN-10, SnO2@MPN-15 and SnO2@MPN-20. (b) XRD patterns of SnO2, SnO2@C-Fe2O3-1, SnO2@C-Fe2O3-3, SnO2@C-Fe2O3-7, SnO2@C-Fe2O3-10, SnO2@C-Fe2O3-15 and SnO2@C-Fe2O3-20. (c) Raman spectra of SnO2@C-Fe2O3-1, SnO2@C-Fe2O3-3, SnO2@C-Fe2O3-7, SnO2@C-Fe2O3-10, SnO2@C-Fe2O3-15 and SnO2@C-Fe2O3-20.

Fig. S5 (a, b) Raman spectra of the pure carbon derived from gallic acid and pyrogallic acid, respectively.

Fig. S6 (a, c, e, g, i and k) SEM images of SnO2@MPN-1, SnO2@MPN-3, SnO2@MPN-7, SnO2@MPN-10, SnO2@MPN-15 and SnO2@MPN-20, respectively. (b, d, f, h, j and l) SEM images of SnO2@C-Fe2O3-1, SnO2@C-Fe2O3-3, SnO2@C-Fe2O3-7, SnO2@C-Fe2O3-10, SnO2@C-Fe2O3-15 and SnO2@C-Fe2O3-20, respectively.

Fig. S7 (a, d) N2 adsorption/desorption isotherm and the corresponding pore size distribution of SnO2, respectively. (b, e) N2 adsorption/desorption isotherm and the corresponding pore size distribution of SnO2@MPN-10, respectively. (c, f) N2 adsorption/desorption isotherm and the corresponding pore size distribution of SnO2@C-Fe2O3-10, respectively.

Fig. S8 (a) XRD patterns of ZnO, ZnO@MPN and ZnO@C-Fe2O3 microflowers. (b, c) SEM and TEM images of ZnO microflowers, respectively. (d) FT-IR spectra of ZnO and ZnO@MPN. (e, f) TG curve and Raman spectrum of ZnO@C-Fe2O3, respectively.

Fig. S9 (a) XRD patterns of LLO, LLO@MPN and LLO@C-Fe2O3 nanoparticles. (b, c) SEM and TEM images of LLO nanoparticles, respectively. (d) FT-IR spectra of LLO and LLO@MPN. (e, f) TG curve and Raman spectrum of LLO@C-Fe2O3, respectively.

Fig. S10 (a) XRD patterns of ZnS, ZnS@MPN and ZnS@C-Fe2O3 hollow spheres. (b, c) SEM and TEM images of ZnS hollow spheres, respectively. (d) FT-IR spectra of ZnS and ZnS@MPN. (e, f) TG curve and Raman spectrum of ZnS@C-Fe2O3, respectively.

Fig. S11 (a) CV curves of the first four cycles at the scan rate of 0.2 mV s-1 of SnO2 in the 0.01-2.5 V range. (b, c) Charge-discharge curves (for the 1st, 2nd, 10th, 50th and 100th cycle at the rate of 0.2 A g-1) of SnO2 and SnO2@C-Fe2O3-10, respectively. (d) The charge-discharge voltage profiles of the SnO2 at different current densities.

Fig. S12 (a) XRD patterns of the C-Fe2O3 derived from pure MPN. (b) Charge-discharge curves (for the 1st, 2nd, 15th and 30th cycle at 0.2 A g-1) of C-Fe2O3. (c) Cycling performance and the corresponding Coulombic efficiencies of C-Fe2O3 at 0.2 A g-1. (d) Long-term cycling performance of C-Fe2O3 at 1 A g-1.

Fig. S13 (a, b) SEM images after 100 cycles at 0.2 A g-1 for SnO2 and SnO2@C-Fe2O3-10, respectively.

Fig. S14 Nyquist plots measured at 2.5 V in the frequency range of 100 kHz-0.01 Hz.

Fig. S15 I-V curves of SnO2 and SnO2@C-Fe2O3-10.

Table S1. The ICP test results of the SnO2@C-Fe2O3-1, SnO2@C-Fe2O3-3, SnO2@C-Fe2O3-7, SnO2@C-Fe2O3-10, SnO2@C-Fe2O3-15 and SnO2@C-Fe2O3-20.

| Material | Sn : Fe | The content of Fe2O3 (wt%) |  |  |
| --- | --- | --- | --- | --- |
| SnO2@C-Fe2O3-1 | 0.9942 : 0.0058 |  | 0.61 |
| SnO2@C-Fe2O3-3 | 0.9843 : 0.0157 |  | 1.64 |
| SnO2@C-Fe2O3-7 | 0.9644 : 0.0356 |  | 3.64 |
| SnO2@C-Fe2O3-10 | 0.9477 : 0.0523 |  | 5.28 |
| SnO2@C-Fe2O3-15 | 0.9496 : 0.0804 |  | 7.98 |
| SnO2@C-Fe2O3-20 | 0.8754 : 0.1246 |  | 12.12 |

Table S2. A comparison of our work and conventional carbon coating methods.

| Coating methods | Coating sources | Advantages | Disadvantages | References |
| --- | --- | --- | --- | --- |
| Metal-phenolic network modification | MPN | ● Precise control ● Simple and fast manipulation ● Programmable process ● No substrate selectivity ● Low cost | ● Solvent consuming | Our work |
| Solution-based polymerization | Dopamine | ● Simple manipulation ● Low cost ● No substrate selectivity | ● Solvent consuming ● Tedious synthesis process ● Hard control on uniform coatings | Adv. Mater. 2017, 29, 1700989. |
| Low-pressure vapor superassembly | MOFs | ● No solvent consuming ● Low cost ● Simple manipulation | ● Substrate material selectivity ● Hard control on precise coatings ● Some requirements of operation condition | Nano Lett. 2017, 17, 7773-7781. |
| Sol-gel method | Citric acid | ● Simple manipulation ● Low cost ● No substrate selectivity | ● Hard control on uniform coatings ● Solvent consuming ● Tedious synthesis process | J. Alloys Compd.2011, 509, 712-718. |
| Chemical vapor deposition | Carbon | ● Precise control ● Uniform deposition ● High quality coatings | ● Complex manipulation ● High cost ● High requirements of operation condition | J. Mater. Chem. 2010, 20, 595-602. |
| Atomic layer deposition | Metal organic compounds | ● Uniform and conformal deposition ● High quality coatings ● Precise control | ● High cost ● Complex manipulation ● High requirements of operation condition | Energy Environ. Sci., 2012, 5, 6872-6879. |

Table S3. Electrochemical performance comparison of various modified SnO2 anode.

| SnO2 anode | Voltage range (V) | Current density (mA g-1) | Cycle number | Residual capacity (mA h g-1) | Capacity retention | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| SnO2@C-Fe2O3-10 | 0.01-2.5 | 200 1000 | 100 1000 | 1203 1003 | 91 % 86 % | Our work |
| Hollow structured SnO2@Si nanospheres | 0.01-1 | 300 | 500 | 778 | 86 % | S1 |
| RGO/SnO2 composites | 0.01-2 | 100 | 200 | 718 | 79 % | S2 |
| Silver nanoparticle-decorated SnO2/NiO nanotubes | 0.01-3 | 1000 | 500 | 826 | 81 % | S3 |
| rGO enwrapping hollow SnO2 nanospheres | 0.01-3 | 100 | 100 | 1107 | 82 % | S4 |
| Sandwiched C@SnO2@C hollow structures | 0.005-3 | 100 | 50 | 933 | 93 % | S5 |
| Ultrafine SnO2/graphene nanocomposite | 0.01-3 | 1000 | 230 | 970 | 97 % | S6 |
| SnO2@Fe2O3 sandwich cubes | 0.01-3 | 100 | 200 | 750.8 | 83 % | S7 |
| Carbon coated SnO2 nanoparticles anchored on CNT | 0.01-2.5 | 1000 | 150 | 930 | 81 % | S8 |
| Okra-like SnO2 encapsulated in nitrogen-doped graphene | 0.01-3 | 200 | 180 | 1041 | 76.4 % | S9 |
| Porous micron-SnO2/C composites | 0.01-3 | 200 | 100 | 954 | 96 % | S10 |

References

1.	T. Ma, X. Yu, H. Li, W. Zhang, X. Cheng, W. Zhu and X. Qiu, Nano Lett., 2017, 17, 3959-3964.

2.	L. Wang, D. Wang, Z. Dong, F. Zhang and J. Jin, Nano Lett., 2013, 13, 1711-1716.

3.	C. Kim, J. W. Jung, K. R. Yoon, D. Y. Youn, S. Park and I. D. Kim, ACS Nano, 2016, 10, 11317-11326.

4.	X. Hu, G. Zeng, J. Chen, C. Lu and Z. Wen, J. Mater. Chem. A, 2017, 5, 4535-4542.

5.	J. Qin, N. Zhao, C. Shi, E. Liu, F. He, L. Ma, Q. Li, J. Li and C. He, J. Mater. Chem. A, 2017, 5, 10946-10956.

6.	W. Chen, K. Song, L. Mi, X. Feng, J. Zhang, S. Cui and C. Liu, J. Mater. Chem. A, 2017, 5, 10027-10038.

7.	Y. Zeng, J. Luo, Y. Wang, L. Qiao, B. Zou and W. Zheng, Nanoscale, 2017, 9, 17576-17584.

8.	C. Ma, W. Zhang, Y. S. He, Q. Gong, H. Che and Z. F. Ma, Nanoscale, 2016, 8, 4121-4126.

9.	X. Zhou, S. Chen, J. Yang, T. Bai, Y. Ren and H. Tian, ACS Appl. Mater. Interfaces, 2017, 9, 14309-14318.

10.	M.-S. Wang, M. Lei, Z.-Q. Wang, X. Zhao, J. Xu, W. Yang, Y. Huang and X. Li, J. Power Sources, 2016, 309, 238-244.