Supporting Information

A Robust Electrospun Separator Modified with in situ Grown Metal-Organic Frameworks for Lithium-Sulfur Batteries

Cheng Zhoua, Qiu Heb, Zhaohuai Lia, Jiashen Menga, Xufeng Honga, Yan Lib, Yan Zhaob, Xu Xu*,a and Liqiang Mai*,a

aState Key Laboratory of Advanced Technology for Materials Synthesis and Processing, International School of Materials Science and Engineering, Wuhan University of Technology, Wuhan 430070, Hubei, China.

*E-mail: xuxu@whut.edu.cn(X. Xu); mlq518@whut.edu.cn(L. Mai).

bState Key Laboratory of Silicate Materials for Architectures, International School of Materials Science and Engineering, Wuhan University of Technology, Wuhan 430070, Hubei, China.

Fig. S1. The SEM images of (a) Co(acac)2 -PAN and (b) PAN nanofibers.

Fig. S2. The elemental mappings of Co(acac)2-PAN nanofibers.

Fig. S3. (a, b) SEM images of rGO-PAN layer; (c) the cross-sectional SEM image of MOF-PAN/rGO-PAN double layered membranes.

Fig. S4. (a) The cross-sectional SEM image of MOF-PAN/rGO-PAN membrane and the corresponding elemental mappings of (b) Co; (c) C; (d) N.

Fig. S5. (a) XRD pattern of the MOF-PAN/rGO-PAN membrane; (b) FTIR spectra of the MOF-PAN, rGO-PAN, and PAN membranes.

Fig. S6. The electrochemical impedance spectroscopic (EIS) curves of Li-S battery assembled with different separators.

Fig. S7. (a) CV curves of the battery with MOF-PAN/rGO-PAN separator; (b) The initial CV profiles of the cells with PP, PAN/rGO-PAN, and MOF-PAN/rGO-PAN separators.

Fig. S8. Galvanostatic charge-discharge profiles of the Li-S batteries with MOF-PAN/rGO-PAN separator at different rates in a potential window from 1.7 to 2.8 V.