Supporting Information

Stabilizing conversion reaction electrodes by MOF derived N-doped carbon shell for highly reversible lithium storage

Fang Liu a,b, Shiyu Liu a, Jiashen Meng a, Fanjie Xia a,b, Zhitong Xiao a, Ziang Liu a, Qi Li*,a , Jinsong Wu*,a,b, Liqiang Maia

aState Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan 430070, China

bNanostructure Research Centre (NRC), Wuhan University of Technology, Wuhan 430070, China

*Correspondence to:wujs@whut.edu.cn; qi.li@whut.edu.cn

Table of Contents:

- Supplementary Figures S1 to S16

- Supplementary Table S1 to S2

- Supplementary Video S1 to S3

- A brief discussion on the surface confinement and heterostructure strategies

Figure S1. The characterizations of Zn2SiO4 nanowires: (a, b) SEM. (c-e) TEM images. (f) SAED pattern. (g-j) SEM image and the corresponding elemental mappings.

Figure S2. TG and DSC curves of the 2-MIM tested in argon conditions.

Figure S3. Optical images of 2-MIM at 25 and 180 °C. This shows the obvious tranformation from solid 2-MIM and liqiud 2-MIM when the environmental temperature increases from 25 to 180 °C.

Figure S4. TEM image (a) and HRTEM image (b) of Zn2SiO4@ZIF-8 nanowires.

Figure S5. Structure variation of Zn2SiO4 (a) and ZnO (b) before and after bond breaking.

Figure S6. SEM images (a, b) and  XRD pattern (c) of ZnO nanoparticals. SEM images (d, e) and  XRD pattern (f) of ZnO@ZIF. SEM images (g-h) and XRD pattern (i) of ZnO@NC.

Figure S7. SEM images of Zn2SiO4@ZIF nanowires at 180C. (a, b) when the reaction time of Zn2SiO4 and 2-Methylimidazole was 3 h. (c, d) when the reaction time of Zn2SiO4 and 2-Methylimidazole was 6 h.

Figure S8. TEM image (a) and SAED pattern (b) of Zn2SiO4@ZIF nanowires. (c) HRTEM image of Zn2SiO4@ZIF nanowires. (d) XPS spectra of Zn2SiO4@ZIF and Zn2SiO4.

Figure S9 (a-f) SEM image and the corresponding EDX mapping images of Zn2SiO4@ZIF nanowires.

Figure S10. Structure characterizations of Zn2SiO4@NC nanowires. (a) Raman spectrum. (b) TG and DSC curves. (c, d) XPS and high-resolution N 1s XPS spectra. (e, f) BET and BJH curves.

Figure S11. SEM image (a), TEM image (b) and XRD pattern (c) of ZnWO4 nanowires. SEM image (d), TEM image (e) and XRD pattern (f) of ZnWO4@ZIF nanowires. SEM image (g), TEM image (h) and XRD pattern (i) of ZnWO4@NC nanowires.

Figure S12. SEM image and the corresponding elemental mappings of ZnWO4@NC nanowires.

Figure S13. (a) The FTIR spectra of ZnWO4@ZIF,  ZIF-8, ZnWO4. (b) Raman spectrum of ZnWO4@NC.

Figure S14. SEM image (a), TEM image (b) and XRD pattern (c) of Zn2TiO4. SEM image (d), TEM image (e) and  XRD pattern (f) of Zn2TiO4@ZIF. SEM image (g), TEM image (h) and XRD pattern (i) of Zn2TiO4@NC.

Figure S15. SEM image and the corresponding elemental mappings of Zn2TiO4@NC.

Figure S16. (a) The FTIR spectra of Zn2TiO4@ZIF, ZIF-8, Zn2TiO4. (b) Raman spectrum of Zn2TiO4@NC.

Figure S17. (a) SEM image of ZnWO4@ZIF. SEM (b) and TEM (c, d) images of ZnWO4@NC. (e-j) SEM image and the corresponding EDX mapping images of ZnWO4@NC nanowire. (k) SEM image of Zn2TiO4@ZIF. SEM (l) and TEM (m, n) images of Zn2TiO4@NC. (o-t) SEM image and the corresponding EDX mapping images of Zn2TiO4@NC.

Figure S18. SEM image (a), TEM image (b) and XRD pattern (c) of Zn2GeO4. SEM image (d), TEM image (e) and  XRD pattern (f) of Zn2GeO4@ZIF. SEM image (g), TEM image (h) and XRD pattern (i) of Zn2GeO4@NC.

Figure S19. The corresponding charge and discharge voltage profiles of Zn2SiO4@NC nanowires at different current densities of 0.1, 0.2, 0.5, 1, 2, 5 A g-1.

Figure S20. a) CV curves of Zn2SiO4@NC nanowires at different scan rates. b) The Nyquist plots of Zn2SiO4@NC nanowires and Zn2SiO4 nanowires.

Figure S21. Schematic illustration of single Zn2SiO4@NC nanowires with efficient electron and Li+ transport and good stress accommodation.

Table S1. A comparison of the current and previous methods for carbon coatings.

| Coating methods | Coating mechanisms | Coating sources | Advantages | Disadvantages | References |
| --- | --- | --- | --- | --- | --- |
| Low-temperature melting synthesis method | Interfacial coordination reaction | MOFs | ● Simple manipulation ● Solvent-free ● High reactivity ● Uniform coatings ● High yield ● Low cost | ● Selected target metal precursors | Our work |
| Solution-based synthesis method | Heterogeneous nucleation growth | MOFs | ● Simple manipulation ● No substrate limitation ● Low cost | ● Solvent consuming ● Low yield ● Hard control on uniform coatings | Chem, 2017, 2, 791-802. |
| Low-pressure vapor superassembly | Interfacial coordination reaction | MOFs | ● Simple manipulation ● Uniform coatings ● High yield ● Low cost | ● Low pressure condition ● Selected target metal precursors | Nano Lett. 2017, 17, 7773-7781. |
| Metal-phenolic network modification | Heterogeneous nucleation growth | MPN | ● Fast formation ● No substrate limitation ● Precise thickness control ● Low cost | ● Solvent consuming ● Low yield | J. Mater. Chem. A, 2018, 6, 18605-18614. |
| Chemical vapor deposition | Epitaxial growth | C2H2 | ● Precise thickness control ● Uniform deposition ● High quality coatings | ● Complex manipulation ● High cost ● Low yield | Adv. Mater. 2017, 29, 1605650. |
| Solution-based polymerization | Epitaxial in situ polymerization | Dopamine | ● Simple manipulation ● No substrate limitation ● Low cost | ● Solvent consuming ● Low yield ● Hard control on uniform coatings | Adv. Mater. 2017, 29, 1700989. |

Table S2. A comparison of our work and other transition metal silicate for LIBs.

| Electrode materials | Modification strategy | Current density (mA g-1) | Cycle number (N) | Reversible capacity (mAh g-1) | Capacity retention (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Zn2SiO4@NC nanowire | Surface confinement | 100 | 100 | 685.2 | 102% | Our work |
| Co2SiO4 naoparticle | - | 100 | 100 | 650 | 130% | [39] |
| Zn2SiO4 nanoparticle | - | 50 | 50 | 293.6 | 85% | [40] |
| Zn2SiO4 microsphere | - | 50 | 20 | 413 | 78.9% | [33] |
| Mn2SiO4/CNT | Hereostructure | 100 | 40 | 466.9 | 119% | [41] |
| Fe2SiO4 | - | 100 | 100 | 800 | 122% | [42] |
| CuSiO3 hollow sphere | - | 100 | 100 | 526 | 82.9% | [43] |
| Mn2SiO4 hollow sphere | - | 100 | 100 | 608 | 91.2% | [43] |
| NiSiOx/RGO | Hereostructure | 50 | 50 | 797 | 100% | [44] |
| Co2SiO4 nanobelts@Carbon composite | Surface confinement | 500 | 100 | 686.4 | 116% | [45] |
| CNT@NiSiOx coaxial nanocables | Hereostructure | 50 | 50 | 489 | 65% | [46] |
| rGO/NiSiO/Ni composites | Hereostructure | 20 | 60 | 478 | 65.4% | [47] |
| Cobalt @ voids @ Ni3Si2O5(OH)4 nanofibers | Hereostructure | 50 | 60 | 432 | 65.5% | [48] |

Video S1. In-situ selected area electron diffraction observation of lithiation of Zn2SiO4 nanowire under a potential bias of -10V. The frame speed is 60-times faster than real time.

Video S2. In-situ TEM observation of lithiation of Zn2SiO4 nanowire under a potential bias of -10V. The frame speed is 60-times faster than real time.

Video S3. In-situ TEM observation of lithiation of Zn2SiO4@NC nanowire under a potential bias of -3V. The frame speed is 18-times faster than real time.

IV. A brief discussion on the surface confinement and heterostructure strategies

Besides surface confinement, heterostructures have also been widely explored for electrode materials. In terms of functions, surface confinement strategy endows the electrode materials with enhanced electric and ionic conductivity, improved materials’ integrity and controllable SEI formation. Generally, the surface confinement layers include carbon materials, Al2O3 and conductive polymers [Adv. Energy Mater. 2017, 7, 1601424; Chem. Commun., 2011, 47, 1384–1404; Science 2017, 358, eaao2808]. As for the heterostructures, they combine the advantages and overcome the limitations of different electrochemically active materials, since a homogeneous single-component electrode material can hardly have the characteristics of high electronic/ionic conductivity and high stability in the electrochemical environment simultaneously. Heterostructures can stabilize the whole structure, enhance high electronic/ionic conductivity and improve the reaction activity. Generally, heterostructured materials can be classified into inorganic–carbon, inorganic–polymer, carbon–polymer, and inorganic–inorganic hybrids [Angew. Chem. Int. Ed. 2016, 55, 3408-3413; Adv. Funct. Mater. 2011, 21, 2439-2445; Energy Environ. Sci. 2017, 10, 1694-1703.]. Both surface confinement and heterostructures strategies will improve electric and ionic conductivity and enhance structure stability. However, while surface confinement strategy can stabilize the SEI and surface confinement layer is generally stable during the electrochemical reaction process, all heterostructures take part in the electrochemical reactions and thus improve the reaction activity.