Supporting information

Self-adaptive FeP@C nanocages for reversible and long-term lithium-ion batteries

Peng Zhoua, Qinyou Ana, Shaohua Zhua, Kwadwo Asare Owusua, Qidong Li*,b,c, Liqiang Mai*,a,d

aState Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan 430070, P. R. China

bEngineering Laboratory for Next Generation Power and Energy Storage Batteries, Tsinghua Shenzhen International Graduate School, Shenzhen 518055, P. R. China

cLaboratory of Advanced Materials, School of Materials Science and Engineering, Tsinghua University, Beijing 100084, P. R. China

dFoshan Xianhu Laboratory of the Advanced Energy Science and Technology Guangdong Laboratory, Xianhu hydrogen Valley, Foshan 528200, P. R. China

*E-mail: mlq518@whut.edu.cn(L. Mai)

*E-mail: li_qidong@126.com(Q. Li)

Fig. S1. FESEM images of (a) uniform Fe2O3 nanocubes, (b) Fe2O3@PRF nanocubes, (c) Fe3O4@C nanocubes and (d) Fe3O4@C nanocages.

Fig. S2. XRD patterns of precursor Fe2O3 nanocubes, Fe3O4@C nanocubes and Fe3O4@C nanocages.

Fig. S3. TEM images of FeP@C nanocages.

Fig. S4. The pore size distributions of B-FeP nanocubes (black), FeP@C-0 nanocubes (blue), and FeP@C nanocages (red).

Fig. S5. CV curves for the first three cycles of B-FeP nanocubes (a), FeP@C-0 nanocubes (b) .

Fig. S6. Charge/discharge curves for the 1st, 5th and 10th cycles at 0.2 A g-1 of B-FeP nanocubes (a), FeP@C-0 nanocubes (b).

Fig. S7. Cycling performance of FeP@C, Fe3O4@C nanocages at 0.5 A g-1.

Fig. S8. The GITT of B-FeP nanocubes (a), FeP@C-0 nanocubes (b) and (c) FeP@C nanocages.

Fig. S9. The corresponding rate charge/discharge curves from 0.2 A g-1 to 10 A g-1 of B-FeP nanocubes (a), FeP@C-0 nanocubes (b) and (c) FeP@C nanocages.

Fig. S10. CV curves and EIS of FeP@C nanocages, (a) CV curves at pristine state and after 200 cycles, (b) EIS at fully charged state after 200 cycles.

Fig. S11. The electrical performance comparison of FeP@C nanocages with other iron-based materials. (a) Specific capacity related to maximal current density; (b) 3D column view of X (current density), Y (capacity retention) and Z (cycle number).

Fig. S12. TEM image of FeP@C after being recharged to 3 V in the first cycle.

Fig. S13. The EIS of B-FeP nanocubes in pristine state (a), FeP@C-0 nanocubes (b) and (c) FeP@C nanocages, (d) the fitting lines of ZRe and w for calculating the Li-ion diffusion coefficients (D).

Fig. S14. FESEM images of (a) B-FeP nanocubes after 10 cycles, (b) FeP@C-0 nanocubes after 50 cycles and (c) FeP@C nanocages after 200 cycles. All of the three samples are tested at a current density of 0.5 A g-1.