Supplementary Data

Ultra-fast and high-stable near-pseudocapacitance intercalation cathode for aqueous potassium-ion storage

Meng Huanga, Xuanpeng Wangb,c,**, Jiashen Menga, Xiong Liua, Xuhui Yaod, Ziang Liua, Liqiang Maia,c,*

a State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, School of Materials Science and Engineering, Wuhan University of Technology, Wuhan 430070, P. R. China.

b Department of Physical Science & Technology, School of Science, Wuhan University of Technology, Wuhan 430070, P. R. China.

c Foshan Xianhu Laboratory of the Advanced Energy Science and Technology Guangdong Laboratory, Xianhu hydrogen Valley, Foshan 528200, China

d Advanced Technology Institute, University of Surrey, Guildford, Surrey GU2 7XH, United Kingdom

* Corresponding authors: Dr. X. Wang (wxp122525691@whut.edu.cn) and Prof. L. Mai (mlq518@whut.edu.cn)

Table S1. The crystallite sizes determined from direct application of the Scherrer equation [1] (without corrections for stress) to selected hkl reflections of sample Ni2Zn1HCF.

| hkl | Crystallite size from Scherrer Equation (nm) |
| --- | --- |
| 111 | 33.5 |
| 200 | 33.7 |
| 220 | 34.0 |
| 400 | 29.9 |
| 420 | 30.3 |
| 440 | 31.5 |
| 600 | 31.9 |
| Average | 32.1 |

Table S2. ICP analysis of the five samples.

| Element Sample | Fe | Ni | Zn | K | Composition |
| --- | --- | --- | --- | --- | --- |
| Ni0Zn3HCF | 2 | 0 | 2.987 | 0.075 | K0.075Zn2.987[Fe(CN)6]2 |
| Ni3Zn3HCF | 2 | 3.060 | 0 | 0.192 | K0.192Ni3.060[Fe(CN)6]2 |
| Zn2Ni1HCF | 2 | 0.854 | 4.405 | 0.102 | K0.102Ni0.854Zn4.405[Fe(CN)6]2 |
| Zn1.5Ni1.5HCF | 2 | 2.035 | 1.487 | 0.328 | K0.328Ni2.035Zn1.487[Fe(CN)6]2 |
| Zn1Ni2HCF | 2 | 2.453 | 0.944 | 0.272 | K0.272Ni2.453Zn0.944[Fe(CN)6]2 |

Fig. S1. EDS mapping images of Ni2Zn1HCF: (a) TEM image, (b) Zn element, (c) Ni element, (d) Fe element, (e) N element, (f) C element, (g) O element and (h) K element.

Fig. S2. TEM (a), and EDS mapping images (b-i) of Ni1.5Zn1.5HCF.

Fig. S3. TEM (a), EDS mapping images (b-i) of Ni1Zn2HCF.

Fig. S4. DTA profiles of (a) Ni2Zn1HCF, (b) Ni1.5Zn1.5HCF, and (c) of Ni1Zn2HCF under Ar atmosphere at the heat rate of 10 K min-1.

Fig. S5. The zoomed in XRD patterns of Fig. 1d.

Fig. S6. SEM images of (a) Zn3[Fe(CN)6]2, (b) Ni3[Fe(CN)6]2, and (c) XRD patterns of Zn3[Fe(CN)6]2 and Ni3[Fe(CN)6]2.

Fig. S7. Nitrogen adsorption-desorption isotherm of (a) Ni2Zn1HCF, (b) Ni1.5Zn1.5HCF and (c) Ni1Zn2HCF, and corresponding pore size distribution of (d) Ni2Zn1HCF, (e) Ni1.5Zn1.5HCF, and (c) Ni1Zn2HCF, respectively.

Fig. S8. Full scan XPS spectra of the pristine materials.

Fig. S9. FTIR spectra (wavenumbers 400-4000 cm-1) of the pristine materials.

Fig. S10. Cycling performances (a) and CV curves (b) of Ni0Zn3HCF and Ni3Zn0HCF.

Fig. S11. (a) Cyclic voltammograms of Ni1.5Zn1.5HCF from 0.1 to 1.0 mV s-1, and (b) the corresponding relationship of the peak current (ip) and the scan rate (mV s-1). (c) Cyclic voltammograms of Ni1.5Zn1.5HCF from 2 to 20 mV s-1, and (d) the corresponding relationship of the peak current (ip) and the scan rate (mV s-1). (e) Cyclic voltammograms of Ni1Zn2HCF from 0.1 to 1.0 mV s-1, and (f) the corresponding relationship of the peak current (ip) and the scan rate (mV s-1). (g) Cyclic voltammograms of Ni1Zn2HCF from 2 to 50 mV s-1, and (h) the corresponding relationship of the peak current (ip) and the scan rate (mV s-1).

Fig. S12. Cycling performances at 333 C in 0.6 M K2SO4 electrolytes using a three-electrode setup with SCE and Pt as reference electrode and counter electrode, respectively.

References

[1] P. Scherrer, N.G.W. Gottingen, Math-Pys. Kl. 2 (1918) 96–100.