Supplementary Information

Engineering d-p Orbital Hybridization through Regulation of interband energy separation for durable aqueous Zn//VO2(B) batteries

Wenwei Zhang#,a, Jianfeng Liu#,b, Wanyue Caic, Min Zhoub, Wenhui Zhongc, Gaofan Xiaob, Ping Luo*,c, Yan Zhao*,d and Qinyou An*,a,e

a State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan 430070, China

b State Key Laboratory of Silicate Materials for Architectures, International School of Materials Science and Engineering, Wuhan University of Technology, 430070, China

c Hubei Provincial Key Laboratory of Green Materials for Light Industry, Hubei Engineering Laboratory of Automotive Lightweight Materials and Processing, New Materials and Green Manufacturing Talent Introduction and Innovation Demonstration Base School of Materials and Chemical Engineering, Hubei University of Technology, Wuhan 430068, China

d College of Materials Science and Engineering, Sichuan University, Chengdu 610065, China

e Hubei Longzhong Laboratory, Wuhan University of Technology (Xiangyang Demonstration Zone), Xiangyang, Hubei, 441000, China.

# W. Zhang and J. Liu contributed equally to this work.

* Corresponding author

E-mail: blueknight_0930@163.com  (P. Luo)

yanzhao@scu.edu.cn  (Y. Zhao)

anqinyou86@whut.edu.cn  (Q. An)

Fig. S1 The comparisons of formation energy in C-, M-, and WVO between interstitial and substitution doping.

Fig. S2 The energy band of  P-, C-, M-, and WVO, respectively.

Fig. S3 The differential charge densities in P-, C-, M-, and WVO after Zn2+ ion insertion within a-c plane.

Fig. S4 (a) Partial density of states for Zn d-orbitals and O13 p-orbitals, and (b) the corresponding pCOHP of the Zn–O13 bond.

Fig. S5 Considered migration paths of Zn2+ diffusions on P-, C-, M-, and WVO at different view.

Fig. S6 Optical photograph of the prepared powder sample (P-, C-, M-, and WVO).

Fig. S7 Typical SEM image and corresponding SEM—Mapping of four samples （P-, C-, M-, and WVO）.

Fig. S8 Typical TEM image and corresponding TEM—Mapping of MVO.

Fig. S9 Typically part XRD pattern of PVO and MVO.

Fig. S10 (a) The Overall XPS spectra for the P-, C-, M-, and WVO. (b-c) The fitted XPS spectra of V 2p and Mo 3d in MVO.

Fig. S11 The dis./charge curves of the four batteries at different current density.

Fig. S12 Cycling performance of the Zn//PVO and Zn//MVO batteries at 10 A g-1.

Fig. S13 (a) GITT potential response curve.

Fig. S14 Charge-discharge GITT curves at 50 mA g-1.Fig. S15 (a) The full XPS spectra of MVO at initial, fully discharged and charged states. (b) Ex-situ Raman spectrum of MVO at the first cycles.

Fig. S16 The diagram of Zn2+ insertion/extraction mechanism in the MVO//Zn batteries.

Table S1 BET specific surface area and pore size parameters

|  | PVO | CVO | MVO | WVO |
| --- | --- | --- | --- | --- |
| BET Surface Area (m²/g) | 12.39 | 20.47 | 46.33 | 8.67 |
| Total Pore Volume (cm3/g) | 0.09 | 0.12 | 0.203 | 0.04 |
| Desorption Average Pore Diameter (nm) | 24.9 | 21.66 | 13.5 | 18.37 |

Table S2 The typical modification of VO2-based cathode for AZIBs

| Cathode | Modification Strategy | Specific Capacity a mA h g−1 at b A g−1 | Cycling performance | Ref. |
| --- | --- | --- | --- | --- |
| Mo-VO2(B) | Metal-ion doping | 325; 0.1 | 264.6 mA h g-1 at 3.0 A g-1; 85% after 3000 cycles | This work |
| NixVO2 | Metal-ion doping | 295.9; 0.1 | 130.6 mA h g-1 at 10.0 A g-1after 2000 cycles | 1 |
| VO2(B) | Morphology structure | 283; 0.1 | About 100 mA h g-1 at 3.0 A g-1; 86% after 3000 cycles | 2 |
| VO2-x(B) | Anion defect | 330; 0.1 | 150 mA h g-1 at 3.0 A g-1; 700 cycles | 3 |
| VO••-rich VO2 (B) | Anion defect | 375; 0.1 | 220 mA h g-1 at 5.0 A g-1; 79.5% after 2000 cycles | 4 |
| VO2/MXene | Composite material | 224.43; 0.2 | 158.3 mA h g-1 at 2.0 A g-1; 80% after 700 cycles | 5 |
| RGO/VO2 | Composite material | 276; 0.1 | About 220 mA h g-1 at 4.0 A g-1；99% after 1000cycles | 6 |
| VO2@V2C | Heterostructure | 190; 0.2 | 68 mA h g-1 at 5.0 A g-1; 81% after 1000 cycles | 7 |
| H--VO2 @CC | Heterostructure and Composite material | 340; 0.1 | 200 mA h g-1 at 4.0 A g-1; 75% after 4500 cycles | 8 |

1.	Cai, Y.; Chua, R.; Kou, Z.; Ren, H.; Yuan, D.; Huang, S.; Kumar, S.; Verma, V.; Amonpattaratkit, P.; Srinivasan, M. ACS Appl. Mater. Interfaces 2020, 12, (32), 36110-36118.

2.	Chen, L.; Ruan, Y.; Zhang, G.; Wei, Q.; Jiang, Y.; Xiong, T.; He, P.; Yang, W.; Yan, M.; An, Q.; Mai, L. Chem. Mater. 2019, 31, (3), 699-706.

3.	Zhang, W.; Xiao, Y.; Zuo, C.; Tang, W.; Liu, G.; Wang, S.; Cai, W.; Dong, S.; Luo, P. ChemSusChem 2021, 14, (3), 971-978.

4.	Li, Z.; Ren, Y.; Mo, L.; Liu, C.; Hsu, K.; Ding, Y.; Zhang, X.; Li, X.; Hu, L.; Ji, D.; Cao, G. ACS nano 2020, 14, (5), 5581-5589.

5.	Shi, Z.; Ru, Q.; Pan, Z.; Zheng, M.; Chi-Chun Ling, F.; Wei, L. ChemElectroChem 2021, 8, (6), 1091-1097.

6.	Dai, X.; Wan, F.; Zhang, L.; Cao, H.; Niu, Z. Energy Storage Mater. 2019, 17, 143-150.

7.	Chen, J.; Xiao, B.; Hu, C.; Chen, H.; Huang, J.; Yan, D.; Peng, S. ACS applied materials & interfaces 2022, 14, (25), 28760-28768.

8.	Luo, P.; Zhang, W.; Cai, W.; Huang, Z.; Liu, G.; Liu, C.; Wang, S.; Chen, F.; Xia, L.; Zhao, Y.; Dong, S.; Xia, L. Nano Res. 2022.