Supplementary Materials for

Constrained C2 adsorbate orientation enables CO-to-acetate electroreduction

Jian Jin1,2,18, Joshua Wicks3,18, Qiuhong Min1,18, Jun Li4,18, Yongfeng Hu5, Jingyuan Ma6,7, Yu Wang6,7, Zheng Jiang6,7, Yi Xu8, Ruihu Lu1,9, Gangzheng Si1, Panagiotis Papangelakis8, Mohsen Shakouri10, Qunfeng Xiao10, Pengfei Ou3, Xue Wang3, Zhu Chen3, Wei Zhang11, Kesong Yu11, Jiayang Song1, Xiaohang Jiang1, Peng Qiu1, Yuanhao Lou1, Dan Wu1, Yu Mao9, Adnan Ozden8, Chundong Wang1, Bao Yu Xia12, Xiaobing Hu13,14, Vinayak P. Dravid13,14, Yun-Mui Yiu15, Tsun-Kong Sham15, Ziyun Wang9, David Sinton8, Liqiang Mai11*, Edward H. Sargent3,16,17*, Yuanjie Pang1*

18These authors contributed equally to this work

*Correspondence and requests for materials should be addressed to Edward H. Sargent, Yuanjie Pang, and Liqiang Mai (ted.sargent@utoronto.ca; yuanjie_pang@hust.edu.cn; mlq518@whut.edu.cn).

This PDF file includes:

Supplementary Text

Figs. S1 to S43

Tables S1 to S31

Table of Contents

Techno-economic analysis	5

Supplementary Figures	13

Supplementary Fig. 1 | Comparison of C-C coupling pathways	13

Supplementary Fig. 2 | Comparison of the bifurcation of *(OH)C=COH → *C=C=O and *(OH)C=COH → *C=COH reaction pathways	14

Supplementary Fig. 3 | Coverage-dependent phase diagram	15

Supplementary Fig. 4 | SEM and size distribution of Cu/Ag-DA nanoparticles.	15

Supplementary Fig. 5 | XPS spectrum of Ag and Cu atoms in Cu/Ag-DA catalysts.	16

Supplementary Fig. 6 | TEM images of the as-synthesized catalysts before and after CORR.	16

Supplementary Fig. 7 | Electrochemically active surface area (ECSA) measurements of Cu/Ag-DA catalysts.	17

Supplementary Fig. 8 | SEM and EDX mapping images of Cu/Ag-DA catalysts.	18

Supplementary Fig. 9 | SEM and EDX images of Cu/Ag-DA catalysts with an annealing temperature of 400 ℃.	18

Supplementary Fig. 10 | TEM characterization of Cu/Ag-DA nanoparticles.	19

Supplementary Fig. 11 | EDS elemental analysis of the gold TEM grid.	20

Supplementary Fig. 12 | XRD patterns of the Cu/Ag-DA catalysts before and after CORR.	20

Supplementary Fig. 13 | XRD patterns of the Cu/M-DA (M = Ag, Au, and NiO) catalysts.	21

Supplementary Fig. 14 | SEM and EDX mapping images of Cu/Au-DA catalysts.	21

Supplementary Fig. 15 | XPS spectrum of Cu/Ni-DA catalysts.	22

Supplementary Fig. 16 | Ex-situ XANES and first-derivative spectra.	22

Supplementary Fig. 17 | Image of custom-built flow-cell for operando X-ray absorption spectroscopy.	23

Supplementary Fig. 18 | Time-dependent operando Cu K-edge XAS of the Cu/Ag-DA catalyst	23

Supplementary Fig. 19 | Operando EXAFS fitting.	24

Supplementary Fig. 20 | In-situ Raman spectroscopy of Cu/Ag-DA and Ag materials.	25

Supplementary Fig. 21 | Schematic of pressurized flow cell system.	26

Supplementary Fig. 22 | NMR spectrum of liquid products from Cu/Ag-DA.	27

Supplementary Fig. 23 | NMR spectrum of liquid products from Cu catalyst (Acetate, Ethanol, n-PrOH)	27

Supplementary Fig. 24 | NMR spectrum of liquid products from Cu/Ag-DA using labeled C.	28

Supplementary Fig. 25 | NMR spectrum of liquid products using Phenol as internal standard.	28

Supplementary Fig. 26 | Gas chromatography analysis of the gas products of CORR.	29

Supplementary Fig. 27 | Low-flow CO electroreduction using Cu/Ag-DA.	30

Supplementary Fig. 28 | CO electroreduction in a pressurized flow cell with varying concentration of KOH electrolyte.	30

Supplementary Fig. 29 | XRD patterns of the Cu/Ag-DA catalysts with varying relative atomic ratios of Cu to Ag	31

Supplementary Fig. 30 | SEM and EDX mapping images of Cu/Ag-DA catalysts prepared with ion implantation.	31

Supplementary Fig. 31 | CO electroreduction performance of Cu/Ag-DA prepared by copper ion implantation.	32

Supplementary Fig. 32 | XRD of the Cu/Ag-DA catalysts with annealing temperature of 400℃	32

Supplementary Fig. 33 | CO electroreduction performance of Cu/Ag-DA annealed at different temperatures	33

Supplementary Fig. 34 | CO electroreduction in a pressurized flow cell with Cu/Au-DA (a-c) and Cu/Ni-DA (d-f) catalyst.	34

Supplementary Fig. 35 | CO electroreduction in a pressurized flow cell using C and Ag control samples.	35

Supplementary Fig. 36 | Photograph of V1 MEA electrolyzer	35

Supplementary Fig. 37 | Stability demonstration of Cu/Ag-DA in the V1 MEA cell over 50 hours	36

Supplementary Fig. 38 | Image of liquid droplets on gas diffusion layer at the end of 50-hour experiment using the V1 pressurized MEA electrolyzer.	36

Supplementary Fig. 39 | Photograph of V2 MEA electrolyzer flow path	36

Supplementary Fig. 40 | Stability demonstration of Cu/Ag-DA in the V2 MEA cell over >800 hours	37

Supplementary Note: Stability Experiments	37

Supplementary Fig. 41 | Stability test of CORR to acetate with Cu/Ag-DA in a flow cell during ~12 hours of electrolysis	38

Supplementary Fig. 42 | Process flow of TRL=3 complexity to electro-synthesize acetic acid from CO.	38

Supplementary Fig. 43 | Techno-economic Analysis of (a) CO-to-potassium acetate and (b) CO-to-acetic acid	39

Supplementary Tables	40

Supplementary Table 1 | Inductive coupled plasma optical emission spectroscopy (ICP-OES) of the as-synthesized Cu/Ag-DA catalysts.	40

Supplementary Table 2 | Cu atomic ratio of catalysts studied in this work	40

Supplementary Table 3 | Cu K-edge EXAFS fitting results of Cu/Ag-DA during CORR at different potentials (vs. RHE).	40

Supplementary Table 4 | Vibrational frequencies of C2 species on Ag35Cu1 with 1 layer of H2O.	41

Supplementary Table 5 | Vibrational frequencies of C2 species derived from 12CO and 13CO on Cu1 Ag35 model slab with 1 layer of H2O.	42

Supplementary Table 6 | Product FEs for Cu/Ag-DA under different applied potential in CORR.	43

Supplementary Table 7 | Comparison of prior CO2/CO-to-acetate reports.	43

Supplementary Table 8 | Raw Data for Fig. 4a	44

Supplementary Table 9 | Raw Data for Fig. 4b	44

Supplementary Table 10 | Raw Data for Fig. 4c	45

Supplementary Table 11 | Raw Data for Fig. 4d	45

Supplementary Table 12 | Raw Data for Fig. 4e	45

Supplementary Table 13 | Raw Data for Supplementary Fig. 28	47

Supplementary Table 14 | Raw Data for Supplementary Fig. 31	47

Supplementary Table 15 | Raw Data for Supplementary Fig. 33	47

Supplementary Table 16 | Raw Data for Supplementary Fig. 34a	48

Supplementary Table 17 | Raw Data for Supplementary Fig. 34b	48

Supplementary Table 18 | Raw Data for Supplementary Fig. 34c	48

Supplementary Table 19 | Raw Data for Supplementary Fig. 34d	48

Supplementary Table 20 | Raw Data for Supplementary Fig. 34e	49

Supplementary Table 21 | Raw Data for Supplementary Fig. 34f	49

Supplementary Table 22 | Raw Data for Supplementary Fig. 37	49

Supplementary Table 23 | Raw Data for Supplementary Fig. 41	49

Supplementary Table 24 | Techno-economic model parameters	51

Supplementary Table 25 | Raw Data for Supplementary Fig. 43	52

Supplementary Table 26 | Free energy corrections.	52

Supplementary Table 27 | Raw Data for Fig 1b, c.	52

Supplementary Table 28 | Raw Data for SI Fig 3.	52

Supplementary Table 29 | Raw Data for Fig 1d. (Coverage Comparison)	53

Supplementary Table 30 | Raw Data for Fig 1d. (Cluster Comparison)	53

Supplementary Table 31 | DFT Models (Source data provided).	54

Supplementary Note: Adsorption of C2 intermediates on low Cu concentration surfaces	61

References	62

# Techno-economic analysis

Our TEA model follows a general outline reported in a previous work1 and all parameters are in Supplementary Table 24. Results are found in Supplementary Table 25 and Supplementary Fig. 43.

We explored the costs to produce 100 tonnes of acetic acid per day (32,850 tonne per year, with a capacity factor of 0.9) over a 20-year factory life. We use an experimentally-derived MEA full-cell voltage of 2.3 V and an experimentally-derived total current density of 100 mA/cm2 from our stability experiments to estimate a real voltage for a prospective industrial electrolyzer.

For the formation of acetate from CO, the chemical equation is:

2CO+3H2O +4e-→CH3COO-+3OH-
2OH-→12O2+H2O +2e-
2CO+OH-+H2O→CH3COO-+O2

Therefore, producing 1 mol of potassium acetate requires 2 mol of CO and 1 mol of KOH. However, the selectivity of CO-to-acetate is less than 100%, so more than 2 mol of CO is required.

Electricity:

The production rate of Potassium Acetate in moles per second is:

KAcO production mols=KAcO production gdayMKAcOgmol= 100×106gday98gmol× 86400sday=11.8 mols

Considering the loss of electrons due to FE below 100%, we find the current required to produce Potassium acetate at the target production rate:

Itotal A=KAcO production mols×n×FFEKAcO= 11.8 mols×4×96485sAmol 91%=5001 kA

We multiply by the experimentally-derived MEA full-cell voltage (2.3 V) to get the power consumed:

Power kW= Itotal× VcellV=11503 kW

We multiply the power consumption by 24 hr to get the energy consumed per 100 tonne of Potassium acetate produced. Multiplying the required energy by the electricity price (2 ¢/kWh) and dividing by the daily output of Potassium acetate, we then get the cost per tonne of Potassium acetate:

Costelectricity$tonne KAcO=Power×24 hr×priceelectricityKAcO production=15503 kW×24 h×0.02$kWh100tonne KAcOday=$55.21tonne KAcO

Electrolyzer Capital Cost:

The reference electrolyzer cost is 450 $/kW 2, and the reference current density is 400 mA cm-2. Multiplying by the unit price of the electrolyzer (450 $/kW) and scaling by the current density (input current density is 100 mA cm-2), we get the total cost of the electrolyzer:

CostTotal Electrolyzer$=Power Consumed kW× CostElectrolyzer $×base current densitymAcm2input current densitymAcm2= 11503 kW×450 $kW×400mAcm2100mAcm2=$20,704,974.26

The above is a one-time total cost of the electrolyzer, which must be converted to a cost per tonne of Potassium acetate. This technique of converting long-term investments into daily costs is used for all capital costs and uses a capital recovery factor (CRF) based on the discount rate i (7%) and the lifetime of the material (20 years).

CRFelectrolyzer=i(1+i)lifetime(1+i)lifetime-1=0.07(1.07)20(1.07)20-1=0.094393

Next, we multiply the total electrolyzer capital cost by the CRF, and divide it by the number of days the plant operates and the daily Potassium acetate production. For all calculations, we assume that the factory has a capacity factor of 0.9.

Costelectrolyzer $tonne KAcO=CRFelectrolyzer×Costelectrolyzer $mAcm2Capacity factor×365daysyear×productiontonne KAcOday=0.094393×$20,704,974.260.9×365daysyear×100tonne KAcOday=$59.49tonne KAcO

While most CO(2) electrolysis literature is reported at atmospheric pressure, this electrolyzer is pressurized to 10-20 atm. Some considerations for a large-scale system include reinforced pipes, reinforced reactor housings, and the need for high-pressure constant flow pumps. To account for additional potential costs for a system at pressure, we refer to the data in ref.3 on biomass to fuel with Fischer-Tropsch. The total one-time pressure cost is assumed to 25% of the cost of the electrolyzer.

Costpressure $tonne KAcO=0.25×Costelectrolyzer $tonne KAcO=$14.87tonne KAcO

Catalyst and Membrane Costs:

For catalyst and membrane costs, we assume 5% of the electrolyzer cost. We use the same procedure as described above to find the cost per tonne of Potassium acetate using a catalyst/membrane lifetime of 5 years:

CRFC&M=i(1+i)lifetime(1+i)lifetime-1=0.07(1.07)5(1.07)20-1=0.24389

CostC&M $tonne KAcO=CRFC&M× CostTotal Electrolyzer $×5%Capacity factor×365daysyear×productiontonne KAcOday=0.24389×$20,704,974.26×5%0.9×365daysyear×100tonne KAcOday=$7.69tonne KAcO

Cathode Gas Separation:

Gaseous side products (H2, C2H4) are separated out of the CO outlet stream to enable the recirculation of unreacted CO. We calculate gaseous separation costs using estimates from a reference pressure-swing adsorption (PSA) system, provided in Supplementary Table 24.

H2 production rate mols=Total Current × FEH2# of electrons*F= 5001202 A×2%2 e-× 96485 Cmol=0.52 mols

H2 Flow Rate m3h=H2 production rate ×R×T P=0.52 mols ×8.314 Jmol K×298 K 10 atm=4.56 m3h

The sum of gaseous side product flow rates and the flow rate of unreacted CO is used to estimate the gaseous separation cost:

Gas Separation Operational Cost $tonne=total flow rate× reference PSA cost×electricity pricetarget output production=10.84m3h×24hday×0.25kWhm3 ×0.02 $kWh÷100 tonne KAcOday=$0.01tonne KAcO

Gas Separation Capital Cost $tonne=reference PSA capital cost×(total flow ratereference capacity)scaling factor×CRFCapacity factor×365×target output production=$1989043×(10.84m3h1000 m3/h )0.7×0.0940.9×365dayyear×100 tonne KAcOday=$0.24tonne KAcO

Liquid Product Separation:

Distillation is a widely used liquid product separation method in CO2RR/CORR4. Recent literature has noted that azeotropic distillation is needed for the separation of acetic acid and water5. Here we fit the results of Aspen Plus Simulation from that work into an equation that depends on the concentration in the outlet stream (Supplementary Table 24). In Supplementary Fig. 37, we obtain a product concentration of 1M after 50 hours and use this value here.

Liquid Separation Operational Cost $tonne=-326.9×ln(product concentration[M]) + 620.95=$620.95tonne KAcO

Liquid Separation Capital Cost $tonne=reference distillation capital cost×(total flow ratereference capacity)scaling factor×CRFCapacity factor×365×target output production=$4162240.00×(66.55 L/min1000 L/min )0.7×0.0940.9×365dayyear×100 tonne KAcOday=$1.80tonne KAcO

Reactants:

Input CO:

First, assuming there are no losses, we calculate the input CO required to produce 100 tonnes of potassium acetate.

CO requiredtonne CO day=i( production ratetonneiday× MCO Mi×molar ratio (CO i) )

Where i = acetate, ethylene, ethanol, n-propanol, and methane

COrequired tonne CO day=100 tonne KAcOday×2898×2+0.79tonne C2H4day ×2828.05×2+(0.52tonne C2H5OHday ×2846.07×2)= 59.3 tonne COday

Now, we multiply this by a market price for CO ($300/tonne)6 and divide by the daily potassium acetate production. Prior literature for the cost to produce CO from a solid oxide electrolysis cell (SOEC) estimates 300-400 $/tonne-CO, including electrolysis and separation7.

Costintput CO$tonne KAcO= $300tonne CO×59.3 tonne COday×1100 tonneKAcOday= $177.81tonne KAcO

Input KOH:

Here we use a KOH price of 790 USD/tonne8, as reported for North America in September 2021. Calculate the required amount of KOH with the same method above:

KOH required tonne KOHday=product output tonne productday× MKOHMproduct×molar ratio (KOHproduct)

KOHrequired tonne KOHday=100 tonne KAcOday× 56.1198.15×1= 57.17 tonne KOH day

Now, multiplying by the KOH price (790 USD/ton) and dividing by our daily production of potassium acetate. The final cost of the input KOH is:

Costinput KOH$tonne KAcO=790 $tonne KOH×57.17 tonne KOHday× 1100 tonneKAcOday=$451.62tonne KAcO

Input water:

Calculate the required amount of water with the same method above:

H2O required tonne H2Oday=product output tonne productday× MH2OMproduct×molar ratio (H2Oproduct)

H2O required tonne H2Oday=100 tonne KAcOday× 1898×1= 18.35 tonne H2O day

Now, multiplying by the cost of water ($5/tonne) and dividing by our daily production of potassium acetate. The final cost of the input water is:

Costinput H2O$tonne KAcO=5 $tonne H2O×21.0 tonne H2Oday× 1100 tonneKAcOday= $0.92tonne KAcO

Total cost of inputs:

Costall inputs $tonne KAcO= CostCO+CostKOH + Costwater=177.81+451.62+0.92=$630.35tonne KAcO

Other operating costs:

To consider the additional operating costs associated with operating the factory (such as labor and maintenance), we have added an additional cost equal to 10% of the electricity cost:

CostsOther operation$tonne KAcO=Costelectricity$tonne KAcO×0.1=$5.52tonne KAcO

Electrolyte cost:

Our electrolyte is 5M KOH. By using a fixed volume ratio of 100 L of electrolyte per square meter of electrolyzer, we can find the total volume of electrolyte needed.

Volumeelectrolyte L=Surface areaelectrolyzer m2×100 Lm2=Totalcurrent ACurrent densitymAcm2×(100cm1m)2×100 Lm2= 5001201 A 0.1Acm2×(100cm1m)2×100 Lm2=500120 L

Masssalt g= molaritysaltmolL×Volumeelectrolyte L×molecular weight gmol=5×406602×56 = 140 308 708 g

Costelectrolyte$=Masssalt tonne×pricesalt$tonne+Volumewater L×pricewater$tonne=140 tonne×790$tonne+ 500120 L×5$tonne=$113,344.48

To get the cost per tonne of potassium acetate, we calculate the new CRF (1.07) by assuming an electrolyte lifetime of one year. Electrolyte costs per tonne of Potassium acetate:

Costelectrolyte $tonne KAcO=CRFelectrolyzer×Costelectrolyte$Capacity factor×365daysyear×productiontonne KAcOday= 1.07×$113,344.480.9×365daysyear×100tonne KAcOday=$3.69tonne KAcO

Total Operational Cost:
This is the combined total of electricity, electrolyte, cathode gas separation, cathode liquid separation, and other operating costs.

CostTotal Operational $tonne KAcO=55.21+3.69+0.01+620.95+5.52=$685.39tonne KAcO

Balance of Plant and Installation:

All capital costs are scaled to estimate the price of peripheral equipment around the electrolyzer and separation units. We assume a balance of plant (BoP) of 50% and a Lang factor of 1. To find our total capital costs, we sum the cost of electrolyzer, membrane & catalyst, and cathode separation capital.

CostTotal Capital $tonne KAcO=59.49+7.69+14.87+0.24+1.80=$84.09tonne KAcO

BOP $tonne KAcO=BOP Factor×CostTotal Capital=0.5×$84.09tonne KAcO=$42.05tonne KAcO

CostInstallation$tonne KAcO=Lang Factor×CostTotal Capital=1×$84.09tonne KAcO=$94.09tonne KAcO

Potassium Acetate Summary:

By summing up all the above costs, we get the cost to produce one tonne of Potassium acetate in an electrolyzer:

CostKAcO= Costinputs+Costoperational + CostCapital+Costinstallation+BOP= 630.35+685.39+84.09+84.09+42.05 =$1525.97tonne KAcO

Prospective Upgrade to Acetic Acid:

Recent reports have shown an in-situ neutralization of potassium acetate to acetic acid9,10 Electrodialysis is another means to convert potassium acetate to acetic acid, and simultaneously recycle the K+ ion in the form of KOH back to the beginning of the process flow. This is important because KOH is a significant input cost.  A conservative energy estimate for electrodialysis is 5 kWh/kg-acid from ref9.

Recent literature has proposed using the cycling of HCl solution to protonate acetate and produce acetic acid5. This has an estimated energy cost of 1.58 kWh kg-1 KOH and we use this value in our calculations herein.

Since the conversion to acetic acid recycles KOH back into the system, we subtract the cost for input KOH from the total, but keep the levelized electrolyte cost.

CostKAcO less KOH= CostKAcO-CostKOH=$1074.35tonne KAcO

For every tonne of acetic acid produce, 1.64 tonnes of potassium acetate are needed.

CostAcetic Acid= (MKAcOMacetic acid)×CostKAcO less KOH+Costelectricity× Energyelectrodialysis=98g-KAcOmol60g-acetic acidmol×1074.35$tonne KAcO+ 0.02$kWh×1580kWhtonne acetic acid=$1772.84tonne Acetic Acid

Energy Costs

We divide the energetic costs for a gate-to-gate CO2-to-acetate process between electrical energy, separation energy and the energy to produce CO from an SOEC.

For electrical energy:

EelectricalGJ/tonne=55.21$tonne0.02$kWh ×0.0036GJkWh= 9.94 GJ/tonne

For separation energy:

Assuming the operational separation cost of $620.95/tonne-Potassium Acetate from the above calculation and the energy for this is provided by renewable electricity, we calculate:

EseparationGJtonne=$620.95 0.02$kWh×0.0036GJkWh=111.8GJtonne

We use a solid oxide electrolysis cell (SOEC) to convert CO2 to CO. The energy was estimated to be 13.49 GJ/ton-CO according to ref7.

ESOECGJ/tonne=CO requiredtonne×13.49GJtonne

For the energy cost analysis of the direct CO2-to-Potassium Acetate pathway described in the main text, we use an anodic CO2 crossover rate of 0.5 mol-CO2/mol-e- and an energy cost of 4 GJ/tonne-CO2 for CO2 removal11.

Anodic crossover CO2KAcO= 0.5mol CO2mol e- 96485Cmol e-×Current[A]×44.1gmol×1 tonne106 g×3600 s×24 h1 day÷100tonneday

EseparationGJtonne=Costseparation 0.02$kWh×0.0036GJkWh+Anodic CrossoverCO2KAcO×4 GJtonne CO2

Therefore, the total energy for production of one tonne of acetate (derived from CO2) can be expressed as follows:

EtotalGJtonne=EelectricalGJtonne+EseparationGJtonne+ESOECGJtonne

Although not reported in the reference CO2-to-Acetate pathway12, the same 0.33 M concentration was used for comparison with the reference CO-to-acetate pathway13.

# Supplementary Figures

Supplementary Fig. 1 | Comparison of C-C coupling pathways from *CO to *(HO)C=COH on a Cu1Ag35(111) surface at a) 0 V and b) -0.6 V.

Supplementary Fig. 2 | Comparison of the bifurcation of *(OH)C=COH → *C=C=O and *(OH)C=COH → *C=COH reaction pathways as an indicator for acetate selectivity across a series of Cu/M-DAs (modeled as Cu1M35, M = Ag, Au, Pd, Pt, Ni) surfaces at a) 0.5 V, b) 0 V, and c) -0.57 V. 0.5 V is the thermodynamic voltage for CO-to-acetate electro-conversion. 0 V is the potential used in the Figure 1b of the main text and is repeated here for comparison. -0.57 V is the applied potential later shown in the manuscript to be optimal for acetate selectivity (91% FE). Since the *C=COH pathway includes an explicit electron transfer and the *CCO pathway does not, it is important to assess the relative difference between them at multiple potentials. We note that the *(OH)C=COH  *C=CO + H2O reaction step is not entirely independent of potential because it is still subject to field effects induced by the electric potential. These effects are captured using the charged water monolayer in the model. The breakeven point at which the relative difference between *C=C=O and *C=COH pathways is 0 occurs at -0.75 V. This voltage is more negative than the voltages where the peak selectivity to acetate is observed (91% FE at -0.57 V and 90% FE at -0.68 V). This agreement between theory and experiment suggests that for all experimentally-relevant applied potentials, the *CCO pathway remains favored over the *C=COH pathway. For experimentally applied voltages even more negative than -0.75 V, we do observe a decline in acetate FE; although this can also be attributed to other confounding factors, such as competition with HER at highly negative potentials and mass transport limitations at high rates.

Supplementary Fig. 3 | Coverage-dependent phase diagram of *CO adsorbed on Ag(111) and Cu1Ag35(111) surfaces.

# Supplementary Fig. 4 | SEM and size distribution of Cu/Ag-DA nanoparticles.

(a) Before and (b) after CORR.

# Supplementary Fig. 5 | XPS spectrum of Ag and Cu atoms in Cu/Ag-DA catalysts.

# Supplementary Fig. 6 | TEM images of the as-synthesized catalysts before and after CORR.

(a) Before and (b) after CORR.

Supplementary Fig. 7 | Electrochemically active surface area (ECSA) measurements of Cu/Ag-DA catalysts. (a) Cyclic voltammetry profiles obtained from Cu/Ag-DA catalyst before and (b) after reaction at sweep rates of 10, 20, 30, 40, 50, 60, 70, 80, 90, and 100 mV·s-1. (c) Double layer capacitance comparison for Cu/Ag-DA catalysts (before and after reaction).

# Supplementary Fig. 8 | SEM and EDX mapping images of Cu/Ag-DA catalysts.

# Supplementary Fig. 9 | SEM and EDX images of Cu/Ag-DA catalysts with an annealing temperature of 400 ℃.

# Supplementary Fig. 10 | TEM characterization of Cu/Ag-DA nanoparticles.

(a) TEM images of the as-synthesized catalysts before CORR. (b-e) EDX and HRTEM images of a single Cu/Ag-DA nanoparticle. (f) TEM images of the as-synthesized catalysts after CORR. (g-j) EDX and HRTEM images of a single Cu/Ag-DA nanoparticle after CORR.

# Supplementary Fig. 11 | EDS elemental analysis of the gold TEM grid.

# Supplementary Fig. 12 | XRD patterns of the Cu/Ag-DA catalysts before and after CORR.

# Supplementary Fig. 13 | XRD patterns of the Cu/M-DA (M = Ag, Au, and NiO) catalysts.

# Supplementary Fig. 14 | SEM and EDX mapping images of Cu/Au-DA catalysts.

# Supplementary Fig. 15 | XPS spectrum of Cu/Ni-DA catalysts.

Supplementary Fig. 16 | Ex-situ XANES and first-derivative spectra. (a) Ex-situ Ag L3-edge XANES and (b) related first derivative spectra of the Cu/Ag-DA catalyst and the bare Ag catalyst before and after CORR. (c) Ex-situ Ag K-edge XANES and (d) related first derivative spectra of Cu/Ag-DA and bare Ag before and after CORR.

# Supplementary Fig. 17 | Image of custom-built flow-cell for operando X-ray absorption spectroscopy.

Supplementary Fig. 18 | Time-dependent operando Cu K-edge XAS of the Cu/Ag-DA catalyst at (a) -0.36 V and (b) -0.66 V.

Supplementary Fig. 19 | Operando EXAFS fitting. Cu K-edge EXAFS fitting results of the Cu/Ag-DA catalyst during CORR at (a) -0.36 V and (b) -0.66 V.

# Supplementary Fig. 20 | In-situ Raman spectroscopy of Cu/Ag-DA and Ag materials.

Spectroscopy data between 250 – 800 cm-1 collected after ∼3 min of electrolysis. Applied potentials in plot are vs. RHE.

Peaks at ∼290, ∼541 and ~620 cm-1 shift to ∼285, ∼534 and ~600 cm-1 when using labelled 13CO gas. These peaks are not present when CO is substituted for an inert gas (N2). 13CO and N2 controls indicate that these correspond to carbon-containing species. Other shifts among peaks in the 320–500 cm-1 region are not easily assessed due to the broad nature of this region. We associate the small peaks from Cu/Ag-DA materials at 285-290 cm-1 and 366 cm-1 with Cu–CO frustrated rotation and Cu–CO stretching vibrations, respectively14–17. A composite triplet of peaks (broad region of 360-540 cm-1) observed from the pure Ag sample is likely to be adsorbed *CO on Ag14,15,17. Similarly, peaks at 418, 440, and 494 cm-1 from Cu/Ag-DA samples are therefore attributed to *CO on Ag. Peaks at 620 cm-1 may be attributed to the out-of-plane rocking mode of (COO-) from locally-produced acetate. The in-plane rocking mode of (COO-) from locally-produced acetate is expected to be at 470 cm-1 (not visible due to the overlap of peaks in this region)18. Contribution to the peak shoulder at ∼595 cm-1 may also be related to the Cu-Oad stretching mode (570–630 cm-1)19.

The strongest peak at 541 cm-1 is close to prior reports of Ag-CO vibrations which typically show a peak at 523-530 cm-1, but comparison to the pure Ag sample suggests this peak is related to another adsorbate. Calculated vibrational frequencies (Supplementary Tables 6 and 7) for a variety of potential adsorbates indicate that *C=C=O or *(OH)C=COH adsorbates may correspond to this peak. Prior literature has hypothesized *C=C=O and *(OH)C=COH to be potentially long-lived species on Cu20.

Broadening of all spectra between 200 and 750 cm-1 may be related to the potential- and OH--dependent libration of water on Ag and Ag-based materials21. Residual copper oxide clusters may also contribute to broadening in this region with reported peaks at 415, 527, and 623 cm-1 15, but a Stark shift with more negative potential suggests that the 620 cm-1 peak is related to an adsorbate and not a significant presence of copper oxide.

# Supplementary Fig. 21 | Schematic of pressurized flow cell system.

Supplementary Fig. 22 | NMR spectrum of liquid products from Cu/Ag-DA. Representative 1H-NMR spectrum of catholyte with Cu/Ag-DA catalyst at -0.57 VRHE and 10 atm in 5 M KOH after 30 minutes of operation. DMSO is used as an internal standard. The peak near 3.33 ppm is assigned to methanol, the solvent used during catalyst deposition.

Supplementary Fig. 23 | NMR spectrum of liquid products from Cu catalyst (Acetate, Ethanol, n-PrOH). Representative 1H-NMR spectrum of catholyte with Cu catalyst at -0.57 VRHE and 1 atm in 5 M KOH after 40 minutes of operation. DMSO is used as an internal standard. The peak near 3.33 ppm is assigned to methanol, the solvent used during catalyst deposition.

Supplementary Fig. 24 | NMR spectrum of liquid products from Cu/Ag-DA using labeled C. Representative 1H-NMR spectrum of catholyte after 13CORR on Cu/Ag-DA GDE at -0.57 V vs. RHE in 5 M KOH. DMSO is used as an internal standard. The peak of acetate has split due to the effect of 13C 22.

Supplementary Fig. 25 | NMR spectrum of liquid products using Phenol as internal standard. Representative 13C-NMR spectrum of catholyte after 13CORR on Cu/Ag-DA GDE at -0.57 VRHE in 5 M KOH. Phenol is used as an internal standard. The peak of acetate has split due to the effect of 13C23, the peaks for acetate at 23.5 and 181.8 ppm, which correspond well with previously published data 24.

# Supplementary Fig. 26 | Gas chromatography analysis of the gas products of CORR.

Supplementary Fig. 27 | Low-flow CO electroreduction using Cu/Ag-DA. 
CO flow of 2 sccm and a potential of -0.7 V vs. RHE in 5 M KOH under 10 atm pressure.

Supplementary Fig. 28 | CO electroreduction in a pressurized flow cell with varying concentration of KOH electrolyte. Experimental data reported with a potential of -0.57 V vs RHE under 10 atm pressure.

Supplementary Fig. 29 | XRD patterns of the Cu/Ag-DA catalysts with varying relative atomic ratios of Cu to Ag.

# Supplementary Fig. 30 | SEM and EDX mapping images of Cu/Ag-DA catalysts prepared with ion implantation.

# Supplementary Fig. 31 | CO electroreduction performance of Cu/Ag-DA prepared by copper ion implantation.

# Supplementary Fig. 32 | XRD of the Cu/Ag-DA catalysts with annealing temperature of 400℃

Supplementary Fig. 33 | CO electroreduction performance of Cu/Ag-DA annealed at different temperatures and measured at a potential of -0.57 V vs RHE in 5 M KOH under 10 atm pressure.

Supplementary Fig. 34 | CO electroreduction in a pressurized flow cell with Cu/Au-DA (a-c) and Cu/Ni-DA (d-f) catalyst. Unless otherwise specified, experimental data reported with a potential of -0.57 V vs RHE in 5 M KOH under 10 atm pressure. The Cu atomic ratios of Cu/Au-DA and Cu/Ni-DA catalysts in variable working conditions are 6.8% and 17%, respectively. (a, d) Effect of Copper atomic ratio; (b, e) Effect of applied potential; (c, f) Effect of CO partial pressure.

Experimental parameters for the control samples were varied in the order of Cu atomic ratio, applied potential, and pressure. For Cu/Au and Cu/Ni materials, the product distribution does not vary significantly when changing the Cu atomic ratio (unlike the Cu/Ag materials). Similarly, the applied potential for the composition carried through from a) to b) and d) to e) does little to change the ratio between acetate FE and the sum of FE from other C2+ products. We observe significant changes when pressure is modulated. For Cu/Au materials, Acetate FE is improved from ∼16% to 60%. We also see a ∼3x improvement in the ratio between acetate and other C2+ products as a result of increasing pressure from 1 atm to 13 atm. On the Cu/Ni surface, the absolute FE also improves, here to ∼45%, but interestingly the ratio (acetate/C2+) does not change significantly. Therefore, improvement to FE on Cu/Ni surfaces is a result of H2 suppression and not necessarily a shift amongst carbon-based products.

In instances where there is significantly more H2 production than with the Cu/Ag-DA materials, we found the total FE to be less than 100%. In the high-pressure electrolyzer, a fraction of H2 is dissolved in the cathode liquid and this fraction is not accounted for amongst the gaseous products measured at the cathode outlet and the liquid products measured at the anode outlet. This fraction of H2 was observed among the cathode liquid products via gas chromatography measurements.

Supplementary Fig. 35 | CO electroreduction in a pressurized flow cell using C and Ag control samples. Cu/C-DA (prepared by ion implantation of Cu onto a carbon black substrate) and an Ag catalyst. Experimental data reported with a potential of -0.57V vs RHE in 5 M KOH.

Supplementary Fig. 36 | Photograph of V1 MEA electrolyzer with a 1 cm2 active geometric area of the flow field on each side.

Supplementary Fig. 37 | Stability demonstration of Cu/Ag-DA in the V1 MEA cell over 50 hours at total current density of 100 mA/cm2 in 5 M KOH at 20 atm. The concentration of acetate in the electrolyte is 1 M (1.7 mol%) at the completion of the 50-hour demonstration.

# Supplementary Fig. 38 | Image of liquid droplets on gas diffusion layer at the end of 50-hour experiment using the V1 pressurized MEA electrolyzer.

Supplementary Fig. 39 | Photograph of V2 MEA electrolyzer flow path with 1 cm2 active geometric area.

a)

a)

b)

b)

Supplementary Fig. 40 | Stability demonstration of Cu/Ag-DA in the V2 MEA cell over >800 hours at total current density of 100 mA/cm2 in 2.5 M KOH at 10 atm. The sampling of liquid products led to voltage changes in some instances, notable changes are highlighted here. (a) Fig. 4e; (b) Voltage response over time. This experiment ended due to a pump failure.

# Supplementary Note: Stability Experiments

Notable improvements from the V1 MEA cell to the V2 MEA cell leading to improved stability:

- Using a Sigracet 39BB gas diffusion layer instead of Freudenburg H14C9 (all other experiments in this work use Freudenburg H14C9, which we found to be stable on a 4-hour time-scale in the 10 atm flow cell and 50-hour time-scale in the 20 atm MEA)

  - Sigracet 39BB materials are 75% thicker (see Thickness), 5.5x stiffer (see Tensile Strength), and less porous (see Air Permeability).

  - These properties result in a substrate more resistant to flooding and more robust over time. By maintaining the position of the triple gas-solid-electrolyte boundary, we improved the stability of the reaction.

| Name | Thickness | Area Weight | Tensile Strength | Through-Plane Air Permeability |
| --- | --- | --- | --- | --- |
| Freudenberg C14H9 | 180 μm | 100 g/m2 | > 1.4 MPa | 30 Gurley sec |
| Sigracet 39BB | 315 μm | 95 g/m2 | 7.7 MPa | 1.5 Gurley sec |

- Re-engineering the gas flow channel of our MEA cell:

  - Using a more shallow flow channel (1 mm reduced to <0.2 mm)

  - Reducing the o-ring size around the flow channel (see Supplementary Fig. 39)

- Optimizing reaction conditions for improved stability by addressing two failure modes of our previous experimental lab set-up:

  - Mitigating against pressure fluctuations in the system by reducing the flow rate of CO gas to 6.8 sccm and reducing the flow rate of electrolyte to 0.5 mL/min

  - Mitigating against gas dissolved in the electrolyte leading to pump failure by continuously supplied fresh electrolyte to avoid the build-up of gas in the line

Supplementary Fig. 41 | Stability test of CORR to acetate with Cu/Ag-DA in a flow cell during ~12 hours of electrolysis at potential of -0.57 V vs RHE in 5 M KOH under 10 atm pressure. At the 5-hour and 9-hour timestamps, the catalyst was removed from the cell, rinsed, dried, and placed back into the cell with the same components. The recovery of performance is indicative of catalyst stability and the increase in H2 is likely attributed to flooding of electrolyte into the gas diffusion layer.

# Supplementary Fig. 42 | Process flow of TRL=3 complexity to electro-synthesize acetic acid from CO.

Supplementary Fig. 43 | Techno-economic Analysis of (a) CO-to-potassium acetate and (b) CO-to-acetic acid compared with the best prior reports of acetate-O2 electrolyzers.

The Reactants component includes the costs for CO (carbon source), water (proton source) and KOH (potassium source) that result in Potassium Acetate. The Electrolyzer Capital component includes the electrolyzer capital costs, catalyst and membrane costs, as well as the cost of electrolyte (not including the electrolyte that is consumed into the product). The Separation component includes both operational and capital costs for gaseous and liquid separation. The Other component includes operational costs that do not fall into other categories (labor, miscellaneous supplies, etc), balance of plant and installation costs.

Data in the first column uses an identical set of performance metrics as this work, with the exception of a Potassium Acetate concentration of 5M instead of 1M. The concentration of acetate at the outlet of the reactor is a critical factor in reducing separation costs5. Higher concentrations have been reported using system-level advances in membrane design13 and anodic oxidation reaction5 selection. These approaches are compatible with the catalyst materials presented herein and would benefit cost reductions further by increasing product concentration.

Supplementary Tables

Supplementary Table 1 | Inductive coupled plasma optical emission spectroscopy (ICP-OES) of the as-synthesized Cu/Ag-DA catalysts. The atomic % of Cu in Cu/Ag-DA catalysts is about 1%.

| Sample | Cu (ppm) | Ag (ppm) | at. %Cu |
| --- | --- | --- | --- |
| Cu/Ag-DA-1 | 0.0676 | 10.8842 | 1.04 |
| Cu/Ag-DA-2 | 0.0631 | 11.206 | 0.95 |

The formula for calculating the %Cu is as follows:

%Cu=Cuppm63.5/(Cuppm63.5+Agppm107.9)

# Supplementary Table 2 | Cu atomic ratio of catalysts studied in this work

| Sample # | Catalyst type | Synthesis method | at. %Cu | Detection method |
| --- | --- | --- | --- | --- |
| 1 | Cu/Ag-DA | Chemical synthesis | 16.4 | XPS |
| 2 | Cu/Ag-DA | Chemical synthesis | 6.7 | XPS |
| 3 | Cu/Ag-DA | Chemical synthesis | 1 | XPS, TEM-EDS, ICP-OES |
| 4 | Cu/Ag-DA | Chemical synthesis | 0.7 | SEM-EDS |
| 5 | Cu/Ag-DA | Chemical synthesis | 0.8 | SEM-EDS |
| 6 | Cu/Ag-DA | Chemical synthesis | 0.1 | SEM-EDS |
| 7 | Cu/Ag-DA | Ion implantation | 2 | SEM-EDS |
| 8 | Cu/Ag-DA | Ion implantation | 34 | SEM-EDS |
| 9 | Cu/Ni-DA | Chemical synthesis | 2.5 | XPS |
| 10 | Cu/Ni-DA | Chemical synthesis | 4.7 | SEM-EDS |
| 11 | Cu/Ni-DA | Chemical synthesis | 17 | SEM-EDS |
| 12 | Cu/Au-DA | Chemical synthesis | 2.5 | SEM-EDS |
| 13 | Cu/Au-DA | Chemical synthesis | 3.1 | SEM-EDS |
| 14 | Cu/Au-DA | Chemical synthesis | 6.8 | SEM-EDS |
| 15 | Cu/Au-DA | Chemical synthesis | 9.8 | SEM-EDS |
| 16 | Cu/Au-DA | Chemical synthesis | 16.2 | SEM-EDS |

# Supplementary Table 3 | Cu K-edge EXAFS fitting results of Cu/Ag-DA during CORR at different potentials (vs. RHE).

| Cu/Ag-DA | Scatter path | Coordination number | Bond length (Å) | ΔE0 (eV) | σ2 (Å2) |
| --- | --- | --- | --- | --- | --- |
| -0.36 V | Cu-C | 1.6 | 2.02 | 2.4 | 0.00531 |
|  | Cu-Cu | 0.4 | 2.46 | -5.3 | 0.00780 |
|  | Cu-Ag | 6.2 | 2.78 | -5.3 | 0.0137 |
| -0.66 V | Cu-C | 1.3 | 2.04 | 4.1 | 0.0109 |
|  | Cu-Cu | 0.6 | 2.43 | -1.8 | 0.0113 |
|  | Cu-Ag | 5.9 | 2.65 | -1.8 | 0.0123 |

Supplementary Table 4 | Vibrational frequencies of C2 species on Ag35Cu1 with 1 layer of H2O. The red, black, and grey arrows represent the plane, in-plane, out-of-plane vibrations.

|  | Vibrational frequencies |
| --- | --- |
| *C=C=O |  |
| *C=COH |  |
| *(HO)C=COH |  |
| *(O)C=COH |  |
| *(O)C=CO |  |

Supplementary Table 5 | Vibrational frequencies of C2 species derived from 12CO and 13CO on Cu1 Ag35 model slab with 1 layer of H2O.

Vibrational frequencies near the experimentally observed 541 cm-1 peak are in red. The competing pathway *C=COH does not have any vibrational frequencies within ±50 cm-1 of this peak.

| Adsorbate | Vibrational frequencies / cm-1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| *12C=12C=O | 1988 | 1210 | 543 | 490 | 309 | 242 | 205 | 192 | 108 |  |  |  |  |  |  |  |  |
| *13C=13C=O | 1919 | 1184 | 526 | 476 | 298 | 236 | 199 | 189 | 107 |  |  |  |  |  |  |  |  |
| *12C=12COH | 3334 | 1840 | 1210 | 972 | 485 | 354 | 326 | 262 | 179 | 143 | 119 | 78 |  |  |  |  |  |
| *13C=13COH | 3334 | 1771 | 1207 | 954 | 483 | 343 | 316 | 253 | 175 | 141 | 117 | 76 |  |  |  |  |  |
| *(O)12C=12CO | 1558 | 1439 | 714 | 638 | 460 | 329 | 298 | 277 | 204 | 187 | 160 | 134 |  |  |  |  |  |
| *(O)13C=13CO | 1406 | 1145 | 976 | 810 | 667 | 606 | 407 | 291 | 286 | 240 | 217 | 184 |  |  |  |  |  |
| *(O)12C=12COH | 3491 | 1401 | 1274 | 1049 | 960 | 745 | 640 | 480 | 390 | 325 | 278 | 261 | 198 | 190 | 176 |  |  |
| *(O)13C=13COH | 3487 | 1361 | 1265 | 1023 | 934 | 725 | 639 | 467 | 387 | 319 | 273 | 255 | 195 | 186 | 172 |  |  |
| *(HO)12C=12COH | 3610 | 3384 | 1447 | 1271 | 1140 | 961 | 950 | 790 | 740 | 578 | 485 | 345 | 300 | 274 | 242 | 168 | 148 |
| *(HO)13C=13COH | 3609 | 3384 | 1404 | 1264 | 1132 | 934 | 928 | 790 | 724 | 576 | 472 | 342 | 294 | 271 | 239 | 166 | 146 |

Supplementary Table 6 | Product FEs for Cu/Ag-DA under different applied potential in CORR. Error bars represent the standard deviation of measurements based on three independent samples.

| Potential (V vs Ag/AgCl) | Potential (V vs RHE) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) | Total current density (mA/cm2) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| -1.275 | -0.23 | 32.6±3.2 | 0 | 0 | 15.1±0.2 | 0 | 26.1±0.1 | 1.6 |
| -1.325 | -0.28 | 70.0±0.7 | 0 | 0 | 7.0±0.8 | 0 | 15.2±1.9 | 4.2 |
| -1.35 | -0.30 | 75.5±2.4 | 0 | 0 | 6.1±0.2 | 0 | 14.6±0.2 | 8.2 |
| -1.40 | -0.34 | 81.4±1.0 | 0 | 0 | 5.6±0.2 | 0.2±0.1 | 7.2±0.7 | 14 |
| -1.50 | -0.43 | 82.5±2.4 | 0 | 0 | 6.0±0.4 | 0.2±0.1 | 9.1±0.5 | 33 |
| -1.60 | -0.51 | 86.7±1.2 | 3.7±0.5 | 0 | 3.7±0.5 | 1.7±0.2 | 2.1±0.5 | 60 |
| -1.70 | -0.57 | 91.2±1.6 | 1.8±0.1 | 0 | 5.2±0.1 | 0.2±0.1 | 1.7±0.3 | 123 |
| -1.85 | -0.68 | 89.6±1.1 | 1.5±0.2 | 0 | 6.9±0.6 | 0.1±0.1 | 1.9±0.1 | 170 |
| -2.00 | -0.79 | 83.6±2.5 | 3.2±0.3 | 0 | 4.1±0.3 | 0 | 2.7±0.4 | 234 |
| -2.30 | -0.99 | 73.7±5.5 | 2.0±0.5 | 0 | 5.2±0.8 | 0 | 9.7±1.5 | 355 |

# Supplementary Table 7 | Comparison of prior CO2/CO-to-acetate reports.

| Catalysts | Pressure | FE (%) | jacetate (mA/cm2) | EE acetate, full-cell (%) | Stability (FE ; time) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Cu/Ag-DA | 10 atm | 85 | 85 | 34 | 85%; 820 h | This work (MEA) |
|  | 10 atm | 81 | 11 | 34 | - | This work (Flow-cell) |
|  |  | 91 | 113 | 27 | - | This work (Flow-cell) |
|  |  | 84 | 196 | 16 | - | This work (Flow-cell) |
|  | 1 atm | 69 | 51 | 21 | - | This work (Flow-cell) |
| Cu–Pd pairs | 1 atm | 70 | 425 | 14a | 43%; 500 h | Nat. Catal. 5, 251–258 (2022).25 |
| Mo oxide clusters modified Cu | 1 atm | 49 | 54 | 6 | - | Appl. Catal. B Environ. 281, (2021).12 |
| Triangular Cu nanosheets | 1 atm | 48 | 96 | 14b | 40%; 3 h | Nat. Catal. 2, 423–430 (2019).26 |
| Cu nanotubes | 1 atm | 43 | 194 | 10 | 35%; 150 h | Proc. Natl. Acad. Sci. 118, (2021).13 |
| Cu | 4 atm | 30 | 44 | 11 | 20%; 24 h | Joule. 3, 240–256 (2019).27 |

a This work did not report an anodic potential of the flow cell, we took the MEA cell data from the article to calculate the full cell energy efficiency (FE of acetate 50%; Potential 3.3V).

b This work did not report an anodic potential so we assume the same value as in our work.

# Supplementary Table 8 | Raw Data for Fig. 4a

Product FEs for Cu/Ag-DA under different CO partial pressures in CORR. Error bars represent the standard deviation of measurements based on three or more independent samples.

| CO partial pressure (atm) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.25 | 23.8±2.5 | 11.0±1.3 | 0 | 6.6±1.4 | 6.4±0.5 | 36.5±4.0 |
| 0.5 | 38.2±2.3 | 9.6±1.4 | 0 | 8.7±0.7 | 7.1±1.1 | 24.7±3.1 |
| 0.75 | 54.0±0.4 | 6.9±0.9 | 0 | 16.8±2.4 | 4.6±0.1 | 12.1±3.9 |
| 1 | 69.1±2.5 | 5.6±0.1 | 0 | 13.6±4.4 | 1.2±0.4 | 8.9±2.5 |
| 5 | 81.2±0.6 | 4.7±0.5 | 0 | 7.5±1.7 | 1.1±0.4 | 4.0±2.1 |
| 10 | 91.2±1.6 | 1.8±0.1 | 0 | 5.2±0.1 | 0.2±0.1 | 1.7±0.3 |
| 13 | 90.2±0.5 | 1.6±0.1 | 0 | 5.6±0.3 | 0.3±0.2 | 2.2±0.3 |

# Supplementary Table 9 | Raw Data for Fig. 4b

Product FEs for Cu/Ag-DA under different applied potentials in CORR. Error bars represent the standard deviation of measurements based on three or more independent samples.

| Potential (V vs RHE) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) | Total Current Density (mA/cm2) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| -0.28 | 70.0±0.7 | 0 | 0 | 7.0±0.8 | 0 | 15.2±1.9 | 4.2 |
| -0.30 | 75.5±2.4 | 0 | 0 | 6.1±0.2 | 0 | 14.6±0.2 | 8.2 |
| -0.34 | 81.4±1.0 | 0 | 0 | 5.6±0.2 | 0.2±0.1 | 7.2±0.7 | 14 |
| -0.43 | 82.5±2.4 | 0 | 0 | 6.0±0.4 | 0.2±0.1 | 9.1±0.5 | 33 |
| -0.51 | 86.7±1.2 | 3.7±0.5 | 0 | 3.7±0.5 | 1.7±0.2 | 2.1±0.5 | 60 |
| -0.57 | 91.2±1.6 | 1.8±0.1 | 0 | 5.2±0.1 | 0.2±0.1 | 1.7±0.3 | 123 |
| -0.68 | 89.6±1.1 | 1.5±0.2 | 0 | 6.9±0.6 | 0.1±0.1 | 1.9±0.1 | 170 |
| -0.79 | 83.6±2.5 | 3.2±0.3 | 0 | 4.1±0.3 | 0 | 2.7±0.4 | 234 |
| -0.99 | 73.7±5.5 | 2.0±0.5 | 0 | 5.2±0.8 | 0 | 9.7±1.5 | 355 |

# Supplementary Table 10 | Raw Data for Fig. 4c

Product FEs for Cu/Ag-DA under different copper atomic ratio in CORR. Error bars represent the standard deviation of measurements based on three or more independent samples.

| at. %Cu | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 100 | 48.5±1.1 | 7.9±2.3 | 9.0±3.1 | 11.0±0.8 | 0 | 15.6±2.0 |
| 17.0 | 66.5±2.3 | 4.9±0.6 | 0 | 7.6±0.9 | 3.7±0.7 | 6.3±1.6 |
| 6.4 | 78.3±4.8 | 2.7±0.3 | 0 | 7.5±0.3 | 2.0±0.3 | 3.1±0.9 |
| 1.0 | 91.2±1.6 | 1.8±0.1 | 0 | 5.2±0.1 | 0.2±0.1 | 1.7±0.3 |
| 0.8 | 77.3±2.2 | 3.5±0.2 | 0 | 2.6±0.2 | 1.1±0.5 | 15.3±3.7 |
| 0.7 | 42.9±0.1 | 0.2±0.1 | 0 | 3.3±0.1 | 2.4±0.2 | 37.1±0.2 |
| 0.1 | 41.9±1.0 | 1.0±0.2 | 0 | 2.4±0.2 | 2.4±0.1 | 39.5±2.3 |
| 0 | 0.6±0.4 | 1.3±0.6 | 0 | 0.9±0.2 | 1.4±0.5 | 92.9±2.5 |

# Supplementary Table 11 | Raw Data for Fig. 4d

Product FEs for Cu/M (Ag, Au, Ni)-DA under different copper atomic ratio in CORR.

| Pressure (atm) | Catalyst | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Cu/Ag | 69.1±2.5 | 5.6±0.1 | 0 | 13.6±4.4 | 1.2±0.4 | 8.9±2.5 |
|  | Cu/Au | 17.0±4.0 | 2.2±0.6 | 0 | 3.2±0.1 | 2.8±1.2 | 63.7±1.3 |
|  | Cu/Ni | 8.6±4.9 | 1.1±0.1 | 0 | 1.9±1.1 | 0 | 69.2±10.0 |
| 5 | Cu/Ag | 81.2±0.6 | 4.7±0.5 | 0 | 7.5±1.7 | 1.1±0.4 | 4.0±2.1 |
|  | Cu/Au | 43.5±0.9 | 3.8±0.1 | 0 | 4.7±0.7 | 0 | 36.2±3.3 |
|  | Cu/Ni | 27.3±5.4 | 5.7±1.4 | 0 | 5.9±1.8 | 0.3±0.1 | 42.7±4.1 |
| 10 | Cu/Ag | 91.2±1.6 | 1.8±0.1 | 0 | 5.2±0.1 | 0.2±0.1 | 1.7±0.3 |
|  | Cu/Au | 59.1±1.0 | 2.6±0.9 | 0 | 4.7±1.0 | 0 | 24.0±1.2 |
|  | Cu/Ni | 41.8±1.4 | 6.9±0.4 | 0 | 6.4±0.7 | 0 | 35.7±1.7 |
| 13 | Cu/Ag | 90.2±0.5 | 1.6±0.1 | 0 | 5.6±0.3 | 0.3±0.2 | 2.2±0.3 |
|  | Cu/Au | 54.8±4.0 | 3.4±0.1 | 0 | 4.2±0.1 | 0.2±0.1 | 24.5±2.7 |
|  | Cu/Ni | 47.4±4.1 | 6.0±0.7 | 0 | 7.7±0.3 | 0.3±0.1 | 28.7±2.3 |

# Supplementary Table 12 | Raw Data for Fig. 4e

Catalyst stability in a MEA cell using Cu/Ag-DA at 10 atm at a current density of 100 mA/cm2.

| Time (h) | Acetate/ (Other C2+) | Acetate (%) | EtOH (%) | C2H4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- |
| 5.0 | 10.4 | 85.8 | 5.5 | 2.8 | 15.1 |
| 17.9 | 11.3 | 82.4 | 3.8 | 3.5 | 13.0 |
| 26.8 | 19.6 | 87.6 | 1.5 | 3.0 | 13.7 |
| 40.1 | 16.4 | 82.0 | 1.8 | 3.2 | 12.8 |
| 49.2 | 16.1 | 80.4 | 2.0 | 3.0 | 13.5 |
| 54.0 | 19.4 | 87.0 | 2.1 | 2.4 | 15.0 |
| 65.6 | 15.6 | 82.0 | 2.2 | 3.1 | 11.8 |
| 72.2 | 13.2 | 82.8 | 3.5 | 2.8 | 12.6 |
| 88.3 | 14.4 | 81.3 | 2.6 | 3.1 | 12.6 |
| 99.9 | 15.9 | 84.4 | 2.2 | 3.1 | 13.2 |
| 112.8 | 18.9 | 79.9 | 1.8 | 2.5 | 12.7 |
| 119.2 | 16.0 | 81.8 | 2.1 | 3.0 | 12.9 |
| 137.1 | 15.8 | 78.9 | 1.8 | 3.2 | 12.5 |
| 145.7 | 16.7 | 82.2 | 2.5 | 2.4 | 13.3 |
| 160.8 | 21.7 | 81.9 | 0.6 | 3.2 | 13.6 |
| 167.8 | 16.1 | 81.0 | 2.3 | 2.8 | 14.4 |
| 184.2 | 16.5 | 80.6 | 2.0 | 2.9 | 16.1 |
| 192.2 | 17.1 | 82.6 | 1.8 | 3.0 | 14.8 |
| 208.0 | 14.0 | 78.5 | 2.5 | 3.1 | 14.6 |
| 216.7 | 13.7 | 80.9 | 2.7 | 3.2 | 13.9 |
| 232.5 | 13.8 | 77.2 | 2.2 | 3.4 | 15.5 |
| 238.8 | 14.1 | 78.4 | 2.3 | 3.3 | 13.6 |
| 254.6 | 16.1 | 82.1 | 2.2 | 2.9 | 19.1 |
| 257.4 | 16.0 | 85.8 | 2.1 | 3.3 | 19.6 |
| 274.9 | 14.1 | 83.9 | 3.2 | 2.8 | 12.6 |
| 281.4 | 13.9 | 80.6 | 2.6 | 3.2 | 19.1 |
| 299.6 | 14.5 | 81.1 | 2.6 | 3.0 | 11.6 |
| 305.3 | 13.9 | 79.0 | 2.6 | 3.1 | 16.0 |
| 322.3 | 12.1 | 77.1 | 3.5 | 2.9 | 12.7 |
| 329.2 | 16.3 | 80.9 | 1.8 | 3.2 | 11.6 |
| 346.9 | 15.8 | 78.8 | 1.5 | 3.5 | 14.6 |
| 353.7 | 15.5 | 81.3 | 2.1 | 3.1 | 12.3 |
| 370.9 | 18.7 | 84.9 | 1.5 | 3.0 | 12.0 |
| 378.1 | 11.7 | 78.8 | 3.2 | 3.5 | 16.1 |
| 395.0 | 14.4 | 81.6 | 2.8 | 2.9 | 12.7 |
| 401.7 | 10.5 | 76.3 | 3.8 | 3.5 | 12.9 |
| 418.6 | 10.8 | 76.9 | 3.6 | 3.5 | 12.3 |
| 426.2 | 12.4 | 79.1 | 3.2 | 3.2 | 11.2 |
| 443.3 | 10.6 | 79.1 | 4.1 | 3.3 | 10.8 |
| 451.0 | 12.1 | 83.8 | 3.2 | 3.7 | 14.1 |
| 466.5 | 12.6 | 81.5 | 3.0 | 3.5 | 10.8 |
| 473.7 | 12.2 | 82.4 | 3.1 | 3.7 | 14.9 |
| 490.4 | 12.1 | 78.7 | 3.4 | 3.1 | 12.6 |
| 497.1 | 12.3 | 79.2 | 3.2 | 3.2 | 15.6 |
| 514.2 | 11.7 | 78.2 | 3.5 | 3.2 | 13.2 |
| 522.0 | 12.9 | 83.1 | 3.3 | 3.2 | 15.0 |
| 538.2 | 12.9 | 82.6 | 3.2 | 3.2 | 10.2 |
| 545.4 | 12.3 | 80.0 | 3.0 | 3.5 | 12.3 |
| 561.7 | 12.0 | 78.1 | 3.4 | 3.1 | 13.5 |
| 572.7 | 9.6 | 78.6 | 4.8 | 3.4 | 16.3 |
| 586.4 | 10.1 | 76.8 | 4.6 | 3.0 | 13.0 |
| 595.6 | 10.5 | 77.3 | 4.2 | 3.1 | 11.2 |
| 613.0 | 12.2 | 81.6 | 2.9 | 3.8 | 15.7 |
| 621.3 | 12.7 | 82.8 | 3.2 | 3.4 | 13.8 |
| 634.2 | 10.0 | 79.3 | 4.6 | 3.4 | 11.6 |
| 641.7 | 10.4 | 76.5 | 4.3 | 3.0 | 13.1 |
| 658.4 | 9.7 | 81.3 | 5.4 | 2.9 | 12.1 |
| 665.1 | 9.4 | 75.7 | 5.0 | 3.0 | 11.5 |
| 682.4 | 12.1 | 75.5 | 3.2 | 3.0 | 11.7 |
| 689.4 | 11.8 | 80.0 | 3.7 | 3.0 | 11.2 |
| 706.4 | 11.7 | 75.0 | 3.5 | 2.9 | 13.0 |
| 729.5 | 11.5 | 76.7 | 3.8 | 2.8 | 13.9 |
| 737.5 | 10.7 | 77.8 | 3.8 | 3.4 | 18.7 |
| 751.0 | 11.8 | 73.8 | 3.5 | 2.8 | 20.5 |
| 757.0 | 11.2 | 78.8 | 4.2 | 2.8 | 20.1 |
| 774.4 | 11.9 | 74.7 | 4.0 | 2.3 | 19.5 |
| 781.9 | 10.8 | 75.6 | 4.4 | 2.6 | 20.0 |
| 798.0 | 10.6 | 76.0 | 4.0 | 3.1 | 20.1 |
| 805.0 | 11.0 | 76.5 | 4.1 | 2.8 | 21.1 |
| 822.0 | 11.8 | 79.9 | 4.1 | 2.6 | 19.8 |

# Supplementary Table 13 | Raw Data for Supplementary Fig. 28

Product FEs for Cu/Ag-DA under different concentration of KOH electrolyte in CORR.

| KOH Concentration (M) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 51.3 | 23.1 | 0 | 13.5 | 0 | 3.1 |
| 2.5 | 77.8 | 8.7 | 0 | 10.0 | 0 | 3.4 |
| 5 | 91.2 | 1.9 | 0 | 5.2 | 0 | 1.7 |
| 7 | 89.9 | 4.0 | 0 | 4.7 | 0 | 2.3 |

# Supplementary Table 14 | Raw Data for Supplementary Fig. 31

CO electroreduction performance of Cu/Ag-DA prepared by copper ion implantation.

| at. %Cu | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 34 | 37.1 | 9.7 | 0 | 2.5 | 1.3 | 43.6 |
| 2.0 | 7.51 | 0 | 0 | 0.6 | 0.2 | 66.7 |

# Supplementary Table 15 | Raw Data for Supplementary Fig. 33

CO electroreduction performance of Cu/Ag-DA annealed at different temperatures.

| Temperature (℃) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| None | 91.2 | 1.8 | 0 | 5.2 | 0.2 | 1.7 |
| 100 | 81.3 | 1.5 | 0 | 6.0 | 0.8 | 2.4 |
| 200 | 73.4 | 2.7 | 0 | 5.9 | 1.3 | 3.9 |
| 400 | 61.1 | 16.0 | 0 | 3.1 | 0.5 | 4.7 |

# Supplementary Table 16 | Raw Data for Supplementary Fig. 34a

Product FEs for Cu/Au-DA under different copper atomic ratio in CORR.

| at. %Cu | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 2.5 | 54.8±2.2 | 3.6±0.4 | 0 | 5.8±1.0 | 0 | 22.0±0.6 |
| 3.1 | 59.3±1.3 | 4.1±1.1 | 0 | 5.6±0.2 | 0.2±0.1 | 16.9±1.2 |
| 6.8 | 59.1±1.0 | 2.6±0.9 | 0 | 4.6±1.0 | 0 | 24.0±1.2 |
| 9.8 | 52.3±3.5 | 3.3±0.2 | 0 | 4.7±0.6 | 0.9±0.1 | 30.4±4.2 |
| 16.2 | 60.5±0.5 | 3.8±0.2 | 0 | 5.6±0.6 | 0.5±0.3 | 24.9±6.1 |

# Supplementary Table 17 | Raw Data for Supplementary Fig. 34b

Product FEs for Cu/Au-DA under different applied potentials in CORR.

| Potential (V vs RHE) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| -0.26 | 41.8±3.8 | 2.2±2.1 | 0 | 4.6±0.7 | 0.05 | 36.8±6.8 |
| -0.46 | 54.6±1.3 | 4.6±1.3 | 0 | 4.3±0.9 | 0.05 | 27.8±2.1 |
| -0.65 | 59.1±1.0 | 2.6±0.9 | 0 | 4.6±1.0 | 0 | 24.0±1.2 |
| -0.86 | 51.3±6.2 | 2.9±0.5 | 0 | 4.0±1.1 | 0.2±0.1 | 27.3±3.4 |

# Supplementary Table 18 | Raw Data for Supplementary Fig. 34c

Product FEs for Cu/Au-DA under different CO partial pressures in CORR.

| CO partial pressure (atm) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 17.0±4.0 | 2.2±0.6 | 0 | 3.2±0.1 | 2.8±1.2 | 63.7±1.3 |
| 5 | 43.5±0.9 | 3.8±0.1 | 0 | 4.7±0.7 | 0 | 36.2±3.3 |
| 10 | 59.1±1.0 | 2.6±0.9 | 0 | 4.7±1.0 | 0 | 24.0±1.2 |
| 13 | 54.8±4.0 | 3.4±0.1 | 0 | 4.2±0.1 | 0.2±0.1 | 24.5±2.7 |

# Supplementary Table 19 | Raw Data for Supplementary Fig. 34d

Product FEs for Cu/Ni-DA under different copper atomic ratio in CORR.

| at. %Cu | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 2.5 | 30.4±2.6 | 7.5±3.4 | 0 | 3.8±0.1 | 7.3±7.1 | 40.5±2.5 |
| 4.7 | 49.4±5.5 | 5.4±0.1 | 0 | 7.3±1.2 | 7.3±1.2 | 17.1±9.8 |
| 17 | 41.8±1.4 | 6.9±0.4 | 0 | 6.4±0.7 | 0 | 35.7±1.7 |

# Supplementary Table 20 | Raw Data for Supplementary Fig. 34e

Product FEs for Cu/Ni-DA under different applied potentials in CORR.

| Potential (V vs RHE) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| -0.44 | 26.7±0.5 | 5.7±0.1 | 0 | 6.8±0.5 | 0 | 48.7±7.2 |
| -0.61 | 41.8±1.4 | 6.9±0.4 | 0 | 6.4±0.7 | 0 | 35.7±1.7 |
| -0.74 | 32.8±1.4 | 6.9±0.2 | 0 | 5.8±1.1 | 0.6±0.3 | 35.1±0.6 |
| -0.88 | 27.6±1.1 | 4.0±0.6 | 0 | 4.9±0.4 | 0.3±0.1 | 42.3±3.4 |

# Supplementary Table 21 | Raw Data for Supplementary Fig. 34f

Product FEs for Cu/Ni-DA under different CO partial pressures in CORR.

| CO partial pressure (atm) | Acetate (%) | EtOH (%) | n-PrOH (%) | C2H4 (%) | CH4 (%) | H2 (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 8.6±4.9 | 1.1±0.1 | 0 | 1.9±1.1 | 0 | 69.2±10.0 |
| 5 | 27.3±5.4 | 5.7±1.4 | 0 | 5.9±1.8 | 0.3±0.1 | 42.7±4.1 |
| 10 | 41.8±1.4 | 6.9±0.4 | 0 | 6.4±0.7 | 0 | 35.7±1.7 |
| 13 | 47.4±4.1 | 6.0±0.7 | 0 | 7.7±0.3 | 0.3±0.1 | 28.7±2.3 |

# Supplementary Table 22 | Raw Data for Supplementary Fig. 37

Catalyst stability in a MEA cell using Cu/Ag-DA at 20 atm.

| Time (h) | Acetate/ (Other C2+) | Acetate (%) | EtOH (%) | C2H4 (%) | H2 (%) | Potential (V) |
| --- | --- | --- | --- | --- | --- | --- |
| 1.8 | 13.9 | 71.9 | 2.7 | 2.4 | 14.3 | 2.21 |
| 13.3 | 16.6 | 73.9 | 2.8 | 1.7 | 15.5 | 2.20 |
| 19.4 | 16.5 | 77.2 | 2.7 | 2.0 | 13.5 | 2.26 |
| 26.5 | 14.6 | 77.3 | 3.6 | 1.7 | 11.7 | 2.26 |
| 35.0 | 16.4 | 83.9 | 3.2 | 1.9 | 12.4 | 2.36 |
| 42.4 | 15.2 | 83.1 | 3.4 | 2.0 | 11.3 | 2.35 |
| 49.6 | 15.2 | 84.4 | 3.4 | 2.1 | 12.5 | 2.44 |

# Supplementary Table 23 | Raw Data for Supplementary Fig. 41

Catalyst stability in a flow cell using Cu/Ag-DA at 10 atm.

| Time (h) | Acetate/ (Other C2+) | Acetate (%) | C2H4 (%) | H2 (%) | Total current density (mA/cm2) |
| --- | --- | --- | --- | --- | --- |
| 0.2 | 13.4 | 90.9 | 5.4 | 1.4 | 116 |
| 0.6 | 12.5 | 89.8 | 5.3 | 2.3 | 119 |
| 1.0 | 12.8 | 90.4 | 5.8 | 3.0 | 119 |
| 1.9 | 12.5 | 89.4 | 5.6 | 4.4 | 119 |
| 2.5 | 12.6 | 88.7 | 5.4 | 6.0 | 118 |
| 3.1 | 11.6 | 86.7 | 6.3 | 6.9 | 116 |
| 3.5 | 11.7 | 84.2 | 6.1 | 8.4 | 115 |
| 3.9 | 10.5 | 81.9 | 5.4 | 11.1 | 114 |
| 4.3 | 10.7 | 80.9 | 5.9 | 12.6 | 114 |
| 4.7 | 10.6 | 79.8 | 6.0 | 13.8 | 113 |
| 5.0 | 10.5 | 79.0 | 6.0 | 14.8 | 112 |
| 5.2 | 12.9 | 91.1 | 5.4 | 3.1 | 111 |
| 5.4 | 13.0 | 91.0 | 5.3 | 2.5 | 109 |
| 5.7 | 12.7 | 90.9 | 5.2 | 3.2 | 108 |
| 5.9 | 12.6 | 89.2 | 5.3 | 4.7 | 106 |
| 6.3 | 11.8 | 88.8 | 5.3 | 6.2 | 105 |
| 6.9 | 12.8 | 86.0 | 5.6 | 7.1 | 104 |
| 6.9 | 12.2 | 86.0 | 5.1 | 8.3 | 102 |
| 7.3 | 11.6 | 84.9 | 5.4 | 8.7 | 101 |
| 7.6 | 11.5 | 82.9 | 5.6 | 10.1 | 105 |
| 8.0 | 11.4 | 80.7 | 5.6 | 10.8 | 111 |
| 8.7 | 12.5 | 79.5 | 5.0 | 11.9 | 106 |
| 8.9 | 12.8 | 79.9 | 5.3 | 12.8 | 108 |
| 9.4 | 13.4 | 88.3 | 5.3 | 5.9 | 108 |
| 9.8 | 12.7 | 87.8 | 5.4 | 6.6 | 110 |
| 10.4 | 12.4 | 85.5 | 5.4 | 7.8 | 112 |
| 10.9 | 12.1 | 81.7 | 5.5 | 9.4 | 114 |
| 11.4 | 11.8 | 81.7 | 5.2 | 12.4 | 118 |
| 11.7 | 13.2 | 79.9 | 4.5 | 13.5 | 115 |
| 12.0 | 13.4 | 81.6 | 4.3 | 14.4 | 114 |

# Supplementary Table 24 | Techno-economic model parameters

| Input Costs | Value | Reference |
| --- | --- | --- |
| CO ($/tonne) | 300.00 | 7 |
| Water ($/tonne) | 5.00 | 7 |
| Electricity ($/kWh) | 0.02 | 7 |
| KOH ($/tonne) | 790.00 | 28 |
| Electrolyte Concentration (M) | 5 | This work |
| Target Production of Potassium Acetate (tonne/day) | 100 | This work |
| Reactor Performance | --- |  |
| Acetate Faradaic Efficiency (%) | 91 | This work |
| Current Density (mA/cm2) | 123 (flow cell); 100 (MEA cell) | This work |
| Cell Voltage (V) | 3.1 (flow cell); 2.3 (MEA cell) | This work |
| Single-Pass Utilization (%) | 70 | This work |
| Product Concentration (%) | 10 |  |
| Plant Parameters | --- |  |
| Reference Electrolyzer Cost ($/kW) | 450 | 2 |
| Reference Current Density (mA/cm2) | 400 | 2 |
| Balance of Plant, BOP (%) | 50 | 7,29 |
| Lang Factor | 1 | 7,29 |
| Capacity Factor (%) | 90 | 7,29 |
| Electrolyzer Lifetime (years) | 20 | 7,29 |
| Catalyst + Membrane Lifetime (years) | 5 | 7,29 |
| Electrolyte Lifetime (years) | 1 | 7,29 |
| Discount Rate (%) | 7 | 7,29 |
| Maintenance Frequency (years-1) | 5 | 7,29 |
| Maintenance Factor (%) | 10 | 7,29 |
| Anolyte Volume (L/m2) | 100 | 7,29 |
| Gas Separation | --- |  |
| PSA Operational Cost (kWh/m3) | 0.25 | 4 |
| PSA Reference Capital Cost ($) | 1 989 043.00 | 4 |
| PSA Reference Capacity (m3/h) | 1000 | 4 |
| PSA Capacity Scaling Factor | 0.7 | 4 |
| Liquid Separation | --- |  |
| Distillation Operational Cost (kWh/kg) | -326.9×ln(concentration[M]) + 620.95 | 5 |
| Distillation Reference Capital Cost ($) | 4,162,240.00 | 4 |
| Distillation Reference Capacity (m3/h) | 1000 | 4 |
| Distillation Capacity Scaling Factor | 0.7 | 4 |

# Supplementary Table 25 | Raw Data for Supplementary Fig. 43

Techno-Economic Analysis of CO-to-acetate.

|  | Reactants ($/tonne) | Electricity ($/tonne) | Electrolyzer Capital ($/tonne) | Pressure ($/tonne) | Separation ($/tonne) | Other ($/tonne) | Total ($/tonne) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| This work | 630.36 | 55.21 | 70.87 | 14.87 | 623.00 | 131.66 | 1525.97 |
| Ref.26 | 662.41 | 141.08 | 87.28 | - | 925.55 | 158.80 | 1966.53 |
| Ref.13 | 671.48 | 295.64 | 51.57 | - | 990.62 | 124.84 | 2126.18 |
| Ref.27 | 737.92 | 168.94 | 144.44 | 31.60 | 625.81 | 296.24 | 1993.82 |
| Ref.25 | 640.27 | 162.68 | 39.75 | - | 925.70 | 83.22 | 1851.61 |

* When acetate concentration was not provided, we assumed the same ratio between product and electrolyte concentration as in our work, i.e., 40 %, we achieve product concentration of 1 M with 2.5 M KOH

# Supplementary Table 26 | Free energy corrections.

| Species | EZPE (eV) | 0298CPdT (eV) | -TS (eV) | G-E (eV) |
| --- | --- | --- | --- | --- |
| CO (g) | 0.144 | 0.039 | -0.610 | -0.427 |
| H2 (g) | 0.301 | 0.023 | -0.404 | -0.079 |
| H2O (l) | 0.567 | 0.050 | -0.216 | 0.401 |
| *CO | 0.188 | 0.081 | -0.121 | 0.148 |
| *H | 0.112 | 0.000 | 0.000 | 0.113 |
| *C=C=O | 0.330 | 0.058 | -0.037 | 0.352 |
| *C=COH | 0.575 | 0.078 | -0.243 | 0.410 |
| *(OH)C=COH | 1.014 | 0.134 | -0.096 | 1.051 |
| *OCCO | 0.239 | 0.107 | -0.085 | 0.261 |
| *OCCOH | 0.534 | 0.119 | -0.095 | 0.559 |

# Supplementary Table 27 | Raw Data for Fig 1b, c.

| Cu1M35 Surface | ΔG*(HO)C=COH→*C=C=O (eV) | ΔG*(HO)C=COH→*C=COH (eV) | ΔG*CO+CO→*OCCO (eV) | ΔG*OCCO→OCCOH (eV) |
| --- | --- | --- | --- | --- |
| Cu1Ag35 | -0.839 | -0.092 | -0.158 | 0.077 |
| Cu1Au35 | -0.510 | 0.265 | 0.331 | 0.024 |
| Cu1Pd35 | 0.626 | 0.091 | 1.965 | 0.513 |
| Cu1Pt35 | 0.622 | 0.193 | 1.518 | 0.008 |
| Cu1Ni35 | 0.629 | -0.353 | 2.356 | -0.328 |

# Supplementary Table 28 | Raw Data for SI Fig 3.

| *CO Surface Coverage | ΔGCO (eV/Surface Atom) @ 1 atm | ΔGCO (eV/Surface Atom) @ 10 atm |
| --- | --- | --- |
| 1/9 | -0.287 | -0.293 |
| 2/9 | -0.231 | -0.244 |
| 3/9 | -0.150 | -0.169 |
| 4/9 | -0.045 | -0.071 |

# Supplementary Table 29 | Raw Data for Fig 1d. (Coverage Comparison)

| Coverage on Cu1Ag35 | ΔG*(HO)C=COH→*C=C=O (eV) | ΔG*(HO)C=COH→*C=COH (eV) | ΔG*(HO)C=COH→*C=C=O - ΔG*(HO)C=COH→*C=COH (eV) |
| --- | --- | --- | --- |
| 2/9 ML | -0.839 | -0.035 | -0.804 |
| 3/9 ML | -1.152 | 0.239 | -1.391 |
| 4/9 ML | -1.156 | 0.033 | -1.189 |

Coverage is defined by the number of carbon atoms among adsorbates per surface atoms in the unit cell in units ML (monolayer).

# Supplementary Table 30 | Raw Data for Fig 1d. (Cluster Comparison)

| Surface | ΔG*(HO)C=COH→*C=C=O (eV) | ΔG*(HO)C=COH→*C=COH (eV) | ΔG*(HO)C=COH→*C=C=O - ΔG*(HO)C=COH→*C=COH (eV) |
| --- | --- | --- | --- |
| Cu1Ag35 | -0.839 | -0.035 | -0.804 |
| Cu2Ag34 | -0.883 | -0.079 | -0.804 |
| Cu3Ag33 | -1.071 | -0.266 | -0.805 |

# Supplementary Table 31 | DFT Models (Source data provided).

|  | Relevant Figure | Slab | Carbon coverage (ML) | Adsorbate | Total Energy (eV) | Side View | Top View |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | SI: 1 | Cu1Ag35 (111) | 1/9 | *CO | -214.272 |  |  |
| 2 | 1c, SI: 1 | Cu1Ag35 (111) | 2/9 | *CO, *CO | -228.918 |  |  |
| 3 | 1b, 1c, 1d | Cu1Ag35 (111) | 2/9 | *C=C=O | -222.524 |  |  |
| 4 | 1b, 1c, 1d | Cu1Ag35 (111) | 2/9 | *C=COH | -225.050 |  |  |
| 5 | 1b, 1c, 1d | Cu1Ag35 (111) | 2/9 | *(OH)C=COH | -236.213 |  |  |
| 6 | 1c | Cu1Ag35 (111) | 2/9 | *CO-CO | -229.073 |  |  |
| 7 | 1c | Cu1Ag35 (111) | 2/9 | *CO-COH | -232.588 |  |  |
| 8 | SI: 1 | Cu1Ag35 (111) | 3/9 | *CO, *CO, *CO | -244.175 |  |  |
| 9 | 1d | Cu1Ag35 (111) | 3/9 | *C=C=O, *CO | -237.101 |  |  |
| 10 | 1d | Cu1Ag35 (111) | 3/9 | *C=COH, *CO | -239.378 |  |  |
| 11 | 1d | Cu1Ag35 (111) | 3/9 | *(OH)C=COH, *CO | -250.815 |  |  |
| 12 | SI: 1 | Cu1Ag35 (111) | 4/9 | *CO, *CO, *CO, *CO | -258.765 |  |  |
| 13 | 1d | Cu1Ag35 (111) | 4/9 | *C=C=O, *CO, *CO | -252.539 |  |  |
| 14 | 1d | Cu1Ag35 (111) | 4/9 | *C=COH, *CO, *CO | -254.679 |  |  |
| 15 | 1d | Cu1Ag35 (111) | 4/9 | *(OH)C=COH, *CO, *CO | -265.910 |  |  |
| 16 | 1b | Cu1Au35 (111) | 2/9 | *CO, *CO | -252.969 |  |  |
| 17 | 1b, 1c | Cu1Au35 (111) | 2/9 | *C=C=O | -245.869 |  |  |
| 18 | 1b, 1c | Cu1Au35 (111) | 2/9 | *C=COH | -248.365 |  |  |
| 19 | 1b, 1c | Cu1Au35 (111) | 2/9 | *(OH)C=COH | -259.886 |  |  |
| 20 | 1b, 1c | Cu1Au35 (111) | 2/9 | *CO-CO | -252.632 |  |  |
| 21 | 1b, 1c | Cu1Au35 (111) | 2/9 | *CO-COH | -256.201 |  |  |
| 22 | 1b | Cu1Ni35 (111) | 2/9 | *CO, *CO | -320.646 |  |  |
| 23 | 1b, 1c | Cu1Ni35 (111) | 2/9 | *C=C=O | -310.645 |  |  |
| 24 | 1b, 1c | Cu1Ni35 (111) | 2/9 | *C=COH | -314.898 |  |  |
| 25 | 1b, 1c | Cu1Ni35 (111) | 2/9 | *(OH)C=COH | -325.800 |  |  |
| 26 | 1b, 1c | Cu1Ni35 (111) | 2/9 | *CO-CO | -318.285 |  |  |
| 27 | 1b, 1c | Cu1Ni35 (111) | 2/9 | *CO-COH | -322.206 |  |  |
| 28 | 1b | Cu1Pd35 (111) | 2/9 | *CO, *CO | -319.442 |  |  |
| 29 | 1b, 1c | Cu1Pd35 (111) | 2/9 | *C=C=O | -309.391 |  |  |
| 30 | 1b, 1c | Cu1Pd35 (111) | 2/9 | *C=COH | -313.198 |  |  |
| 31 | 1b, 1c | Cu1Pd35 (111) | 2/9 | *(OH)C=COH | -324.544 |  |  |
| 32 | 1b, 1c | Cu1Pd35 (111) | 2/9 | *CO-CO | -317.471 |  |  |
| 33 | 1b, 1c | Cu1Pd35 (111) | 2/9 | *CO-COH | -320.552 |  |  |
| 34 | 1b | Cu1Pt35 (111) | 2/9 | *CO, *CO | -354.340 |  |  |
| 35 | 1b, 1c | Cu1Pt35 (111) | 2/9 | *C=C=O | -345.272 |  |  |
| 36 | 1b, 1c | Cu1Pt35 (111) | 2/9 | *C=COH | -348.973 |  |  |
| 37 | 1b, 1c | Cu1Pt35 (111) | 2/9 | *(OH)C=COH | -360.421 |  |  |
| 38 | 1b, 1c | Cu1Pt35 (111) | 2/9 | *CO-CO | -352.817 |  |  |
| 39 | 1b, 1c | Cu1Pt35 (111) | 2/9 | *CO-COH | -356.403 |  |  |
| 40 | 1d | Cu2Ag34 (111) | 2/9 | *C=C=O | -223.399 |  |  |
| 41 | 1d | Cu2Ag34 (111) | 2/9 | *C=COH | -225.923 |  |  |
| 42 | 1d | Cu2Ag34 (111) | 2/9 | *(OH)C=COH | -237.042 |  |  |
| 43 | 1d | Cu3Ag33 (111) | 2/9 | *C=C=O | -224.488 |  |  |
| 44 | 1d | Cu3Ag33 (111) | 2/9 | *C=COH | -227.012 |  |  |
| 45 | 1d | Cu3Ag33 (111) | 2/9 | *(OH)C=COH | -237.943 |  |  |
| 46 | SI: 2 | Cu1Ag35 (111) | 2/9 | *COH, *CO | -231.429 |  |  |
| 47 | SI: 2 | Cu1Ag35 (111) | 2/9 | *COH, *COH | -233.447 |  |  |

# Supplementary Note: Adsorption of C2 intermediates on low Cu concentration surfaces

Examining the C2 adsorbates on Cu1Ag35 surfaces (rows 3-7 in Supplementary Table 28 and the source data provided), we observe that for all bidentate C2 adsorbates, one carbon adsorbs to the Cu atom or in a Cu-Ag bridge site, and the other carbon adsorbs to a Cu-Ag bridge site or a Cu-Ag-Ag hollow site. Based on this data, it does not appear that a single C2 adsorbate is adsorbed entirely and only to the Cu atom. Ag alone is a traditionally weak binder of *CO and multi-carbon adsorbates – hence the typical production of CO from CO2 electroreduction on Ag catalysts. Pure Ag bind *CO so weakly that it desorbs and does not permit further reduction. Here we use CO as a reactant, and we do not expect it to adsorb in regions of the catalyst that only have Ag. However, this assumption should not hold in the presence of Cu atom(s), which modulate the adsorption strength of nearby Ag atoms. With this in mind, Cu atoms and their neighboring Ag atoms are the regions of the catalyst where we expect electrocatalysis to proceed.

# References

1.	Sisler, J. et al. Ethylene Electrosynthesis: A Comparative Techno-economic Analysis of Alkaline vs Membrane Electrode Assembly vs CO2-CO-C2H4Tandems. ACS Energy Lett. 6, 997–1002 (2021).

2.	Ruth, M.; Mayyas, A.; Mann, M. National Renewable Energy Laboratory. Manufacturing Competitiveness Analysis for PEM and Alkaline Water Electrolysis Systems. Fuel Cell Semin. Energy Expo (2017).

3.	Hamelinck, C. N., Faaij, A. P. C., den Uil, H. & Boerrigter, H. Production of FT transportation fuels from biomass; technical options, process analysis and optimisation, and development potential. Energy 29, 1743–1771 (2004).

4.	Jouny, M., Luc, W. & Jiao, F. General Techno-Economic Analysis of CO2 Electrolysis Systems. Ind. Eng. Chem. Res. 57, 2165–2177 (2018).

5.	Overa, S. et al. Enhancing acetate selectivity by coupling anodic oxidation to carbon monoxide electroreduction. Nat. Catal. 5, 738–745 (2022).

6.	Kibria, M. G. et al. Electrochemical CO2 Reduction into Chemical Feedstocks: From Mechanistic Electrocatalysis Models to System Design. Adv. Mater. 1807166, 1–24 (2019).

7.	Ozden, A. et al. Cascade CO2 electroreduction enables efficient carbonate-free production of ethylene. Joule 5, 706–719 (2021).

8.	Brynolf, S., Taljegard, M., Grahn, M. & Hansson, J. Electrofuels for the transport sector : A review of production costs. Renew. Sustain. Energy Rev. 81, 1887–1905 (2018).

9.	Huang, C., Xu, T., Zhang, Y., Xue, Y. & Chen, G. Application of electrodialysis to the production of organic acids: State-of-the-art and recent developments. J. Memb. Sci. 288, 1–12 (2007).

10.	Lopez, A. M. & Hestekin, J. A. Separation of organic acids from water using ionic liquid assisted electrodialysis. Sep. Purif. Technol. 116, 162–169 (2013).

11.	Alerte, T. et al. Downstream of the CO2 Electrolyzer: Assessing the Energy Intensity of Product Separation. ACS Energy Lett. 6, 4405–4412 (2021).

12.	Zang, D. et al. Interface engineering of Mo8/Cu heterostructures toward highly selective electrochemical reduction of carbon dioxide into acetate. Appl. Catal. B Environ. 281, 119426 (2021).

13.	Zhu, P. et al. Direct and continuous generation of pure acetic acid solutions via electrocatalytic carbon monoxide reduction. Proc. Natl. Acad. Sci. USA. 118, (2021).

14.	Gao, J. et al. Selective C-C Coupling in Carbon Dioxide Electroreduction via Efficient Spillover of Intermediates As Supported by Operando Raman Spectroscopy. J. Am. Chem. Soc. 141, 18704–18714 (2019).

15.	Herzog, A. et al. Operando Investigation of Ag-Decorated Cu2O Nanocube Catalysts with Enhanced CO2 Electroreduction toward Liquid Products. Angew. Chemie - Int. Ed. 60, 7426–7435 (2021).

16.	Moradzaman, M. & Mul, G. In Situ Raman Study of Potential-Dependent Surface Adsorbed Carbonate, CO, OH, and C Species on Cu Electrodes During Electrochemical Reduction of CO2. ChemElectroChem 8, 1–9 (2021).

17.	Ichiro Oda, Hirohito Ogasawara,  and M. I. Carbon Monoxide Adsorption on Copper and Silver Electrodes during Carbon Dioxide Electroreduction Studied by Infrared Reflection Absorption Spectroscopy and Surface-Enhanced Raman Spectroscopy. Langmuir 12,1094–1097 (1996).

18.	Quilès, F. & Burneau, A. Infrared and Raman spectra of alkaline-earth and copper(II) acetates in aqueous solutions. Vib. Spectrosc. 16, 105–117 (1998).

19.	Zhao, Y. et al. Speciation of Cu Surfaces during the Electrochemical CO Reduction Reaction. J. Am. Chem. Soc. 142, 9735–9743 (2020).

20.	Cheng, T., Fortunelli, A. & Goddard, W. A. Reaction intermediates during operando electrocatalysis identified from full solvent quantum mechanics molecular dynamics. Proc. Natl. Acad. Sci. USA. 116, 7718–7722 (2019).

21.	Itoh, T., Kajita, T., Maeda, T. & Kasuya, A. In situ surface-enhanced raman analysis of water librationon silver electrode in various alkali hydroxide aqueous solutions. Electrochemistry 82, 396–400 (2014).

22.	Karapinar, D. et al. Electroreduction of CO2 on Single-Site Copper-Nitrogen-Doped Carbon Material: Selective Formation of Ethanol and Reversible Restructuration of the Metal Sites. Angew. Chemie - Int. Ed. 58, 15098–15103 (2019).

23.	Lum, Y. & Ager, J. W. Evidence for product-specific active sites on oxide-derived Cu catalysts for electrochemical CO2 reduction. Nat. Catal. 2, 86–93 (2019).

24.	Chatterjee, T., Boutin, E. & Robert, M. Manifesto for the routine use of NMR for the liquid product analysis of aqueous CO2 reduction: From comprehensive chemical shift data to formaldehyde quantification in water. Dalt. Trans. 49, 4257–4265 (2020).

25.	Ji, Y. et al. Selective CO-to-acetate electroreduction via intermediate adsorption tuning on ordered Cu–Pd sites. Nat. Catal. 5, 251–258 (2022).

26.	Luc, W. et al. Two-dimensional copper nanosheets for electrochemical reduction of carbon monoxide to acetate. Nat. Catal. 2, 423–430 (2019).

27.	Ripatti, D. S., Veltman, T. R. & Kanan, M. W. Carbon Monoxide Gas Diffusion Electrolysis that Produces Concentrated C2 Products with High Single-Pass Conversion. Joule 3, 240–256 (2019).

28.	Caustic Potash Price Trend and Forecast. https://www.chemanalyst.com/Pricing-data/caustic-potash-1212. 1–2 (2021).

29.	Wang, X. et al. Efficient electrosynthesis of n-propanol from carbon monoxide using a Ag–Ru–Cu catalyst. Nat. Energy 7, 170–176 (2022).