Porous Carbonized graphene-embedded fungus film as an interlayer for superior Li-S batteries

Liyuan Chai, a, b, 1 Jiexi Wang,a, c, 1 Haiying Wang,a, b, 1 Liyuan Zhang,a, e * Wanting Yu,d Liqiang Maic, *

a School of Metallurgy and Environment, Central South University, Changsha, 410083, P. R. China

b Chinese National Engineering Research Center for Control & Treatment of Heavy Metal Pollution, Central South University, Changsha, 410083, P. R. China
c State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan, 430070, P. R. China

d Department of Environmental Monitoring, Changsha Environmental Protection College, Changsha 410004, China

e Environmental Engineering Research Centre, Department of Civil Engineering, the University of Hong Kong, Hong Kong, P. R. China

1 Liyuan Chai, Jiexi Wang and Haiying Wang contributed equally to this work.

* Corresponding Author, zhang_livyl@csu.edu.cn, lyzhk@hku.hk (L. Zhang)

mlq518@whut.edu.cn (L. Mai)

Figure S1. Optical microscope image of fungus. This image was acquired by optical microscope. The sample was stained by lactophenol blue solution.

Figure S2. SEM image of the fungus film.

Figure S3. Free standing film from the vacuum filtration of the fungus hyphae.

Figure S4. Raman spectra of graphene nanosheets and fungus hyphae.

Graphene nanosheets

Fungus hyphae

Figure S5. Raman spectrum of the fungus-derived carbon.

This sample was prepared by otherwise the same carbonization condition only without using graphene nanosheets. The peak at ~1340 cm-1 is much broader than that of GFC film mentioned in the main text.

Figure S6. FTIR spectrum of the GFC film.

Figure S7. Comparison of the conductivity of the biomass-derived carbon.

| Materials | Conductivity (S cm-1) | Carbonization temperature (oC) | References |
| --- | --- | --- | --- |
| Carbon aerogel | 0.1 | 950 | RSI-7-1 |
| Bacterial cellulose-derived carbon | 0.41 | 1450 | RSI-7-2 |
| Carbon fiber aerogel | 1.23 | 800 | RSI-7-3 |
| Porous Carbonized graphene-embedded fungus film | 0.71 | 800 | This work |

References

[RSI-7-1] Nicolas Brun, et al. Green Chem., 2013, 15, 2514.

[RSI-7-2] Hai-Wei Liang, et al. NPG Asia Mater., 2012, 4, e19.

[RSI-7-3] Liyuan Zhang, et al. Green Chem., 2014, 16, 3926.

Figure S8. The pore distribution of the GFC film.

Figure S9. Comparison of the performance of Li-S batteries with inserting biomass-derived carbon membrane.

| Materials | Capacity (mAh g-1) | Cycles | Rate (C) | References |
| --- | --- | --- | --- | --- |
| Carbon fiber membrane | 630 | 100 | 0.5 | RSI-8-1 |
| Carbonized paper | 890 | 100 | 1.0 | RSI-8-2 |
| Leaf-derived carbon | 829 | 100 | 0.5 | RSI-8-3 |
| Cassava-derived carbon | 811 | 100 | 0.5 | RSI-8-4 |
| Carbonized filter paper | 560 | 50 | 1.0 | RSI-8-5 |
| Carbonized eggshell | 1000 | 100 | 0.2 | RSI-8-6 |
| Porous Carbonized graphene-embedded fungus film | 887 | 100 | 1.0 | This work |

References

[RSI-8-1] Liyuan Zhang, et al. Green Chem., 2014, 16, 3926.

[RSI-8-2] Sheng-Heng Chung, et al. Chem. Commun., 2014, 50, 4184.

[RSI-8-3] Sheng-Heng Chung, et al. ChemsusChem, 2014, 7, 1655.

[RSI-8-4] Furong Qin, et al. New J. Chem., 2014, 38, 4549.

[RSI-8-5] Kai Zhang, et al. Mater. Lett., 2014, 121, 198.

[RSI-8-6] Sheng-Heng Chung, et al. Adv. Mater., 2013, 26, 1360.

Figure S10. Homogeneous sulfur distribution in the interlayer