Supporting Information

Graphene Decorated Vanadium Oxide Nanowire Aerogel for Long-Cycle-Life Magnesium Battery Cathodes

Qinyou An,1 Yifei Li,1 Hyun Deog Yoo,1 Shuo Chen,2, 3 Qiang Ru,1 Liqiang Mai,4,* and Yan Yao1, 3,*

1 Department of Electrical and Computer Engineering & Materials Science and Engineering Program, University of Houston, Houston, TX 77204, USA

2 Department of Physics, University of Houston, Houston, TX 77204, USA

3 Texas Center for Superconductivity, University of Houston, Houston, TX 77204, USA

4 State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan 430070, China

Correspondence authors: mlq518@whut.edu.cn (L. Mai), yyao4@uh.edu (Y. Yao)

Materials synthesis:

Synthesis of the rGO: The rGO was synthesized through a modified Hummer method.S1,S2

Synthesis of V2O5 sols: The V2O5 sols were prepared by a melt quenching process. V2O5 power (20 g) was heated to 800 °C in a ceramic crucible and was kept for 20 min. Then, the molten liquid was quickly poured into 1 L distilled water while stirring and a brownish solution was formed immediately. The solution was allowed to heat to the boiling point and then cool down to room temperature. After filtration and aging for more than 3 days, brownish V2O5 sols were obtained. The concentration of the V2O5 sols was calculate by weighting the residual mass after drying the sols in 180 °C for 24 hrs.

Figure S1. SEM image of the VOG-1 nanocomposite showing the highly interconnected and porous 3D structural of aerogels.

Figure S2. SEM images of the rGO nanosheets at (a) low magnification and (b) high magnification. Large rGO nanosheets are composed of graphene nanoflakes (0.5-2.0 μm) exfoliated from micrometer-sized graphites.

Figure S3. Thermogravimetric (TG) curve of VOG-1. The TG analysis was carried out at a heating rate of 10 ⁰C min-1 in N2 atmosphere. 12.3% weight loss corresponds to the crystal water loss. Thus the formula of VOG-1 is determined as V2O5·1.42H2O.

Figure S4. SEM images of (a) VOG-2 and (b) VOG-3. The highly interconnected and porous aerogels structure are preserved after annealing at 300 ⁰C in argon for VOG-2 or in air for VOG-3.

Figure S5. (a) Nitrogen adsorption-desorption isotherm and (b) Raman spectrum of VOG-1. Inset in (a) corresponds to the pore-size-distribution curve. BET surface area of VOG-1 is 28.5 m2 g-1.

Figure S6  The XPS spetra of VOG-1.

Figure S7. SEM images of V2O5·1.35H2O nanowires. V2O5·1.35H2O exhibits interconnected nanowires structure.

References

S1. Hummers, W. S., Jr.; Offeman, R. E. J. Am. Chem. Soc. 1958, 80, 1339-1339.

S2. Liang, Y.; Li, Y.; Wang, H.; Zhou, J.; Wang, J.; Regier, T.; Dai, H. Nat. Mater. 2011, 10, 780-786.

S3. Su, D.; Wang, G. ACS Nano 2013, 7, 11218-11226.