Supporting Information

Self-sacrificed synthesis of three-dimensional Na3V2(PO4)3 nanofiber network for high-rate sodium-ion full batteries

Wenhao Ren, Zhiping Zheng, Chang Xu, Chaojiang Niu, Qiulong Wei, Qinyou An,* Kangning Zhao, Mengyu Yan, Mingsheng Qin and Liqiang Mai*

State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan 430070, China

*Correspondence authors: mlq518@whut.edu.cn; anqinyou@whut.edu.cn

Synthesis of NaTi2(PO4)3/C anode:

First, C10H14O5Ti (2 mmol) were added in 20 ml EG with stirring for 0.5 h to form uniform light yellow solution. Then, CH3COONa (4 mmol), H3PO4 (0.19 ml), citric acid (2 mmol) and 20 ml water were dissolved in above solution with stirring at 80°C for 24 h. The solution was then dried at 70 °C in an air oven to get the gray power. In the end, the NaTi2(PO4)3/C was obtained from the precursor via preheating it at 400 °C for 4 h followed by annealing at 700 °C for 8 h in argon atmosphere with a heating rate of 5 °C min-1.

Figure S1. SEM images of the samples with pure water (a) and pure DMF (b) as the solvent and the other experiment conditions are the same.

Figure S2. The detailed morphological evolution process from microflower to 3D nanofiber network. SEM images of the samples with low and high magnification after solvothermal reaction for 6 (a,b), 10 (c,d), 15 (e,f) and 20 h (g,h).

Figure S3. SEM images of the NVP-M before (a) and after (b) annealing at 700 ºC. The TEM (c) and HRTEM (d) images of the NVP-M after annealing at 700 ºC.

Figure S4. TEM images of the NVP-F after annealing at 700 ºC. The red circle presents the connected region of nanofiber.

Figure S5. XRD patterns of the samples after solvothermal reaction for 3, 10 and 20 h.

Figure S6. Nitrogen adsorption–desorption isotherm of NVP-M.

Figure S7. XPS pattern of NVP-F after calcination at 700 °C in argon atmosphere.

Figure S8. The charge-discharge curves of NVP-F at different cycles at 10 C.

Figure S9. XRD patterns of homemade NaTi2(PO4)3.

Figure S10. SEM image of homemade NaTi2(PO4)3 and the corresponding EDS elemental mapping.

Figure S11. (a) Cycling performance and coulombic efficiency of homemade NaTi2(PO4)3. (b) Galvanostatic charge-discharge curves of NVP-F at different cycles.

Table S1. The fitting values based on the EIS data.

| Cell state | Rs(ohm) | Rct(ohm) |
| --- | --- | --- |
| NVP-F full cell after 2 cycles | 4.49 | 39.64 |
| NVP-F full cell after 10 cycles | 4.00 | 41.45 |
| NVP-F full cell after 50 cycles | 3.69 | 42.60 |
| NVP-F full cell after 100 cycles | 3.61 | 48.99 |
| NVP-F full cell after 200 cycles | 2.87 | 53.93 |

Figure S12. Charge-discharge curves of NVP‖1 M NaClO4 /EC + DMC + FEC‖NTP full cell as the current densities increase from 1 C to 50 C at a potential window between 0.7 and 2.4 V versus Na+/Na.

Figure S13. Ragone plots of the NVP-F based full cell.

Figure S14. (a) Overcharge tolerance test of the NVP-F cycled at 5 C. (b) The corresponding charge-discharge curves.

Figure S15. Schematic illustration of the Na ion insertion/deinsertion process in 3D nanofiber network (a) and microflower structure (b).

Figure S16. The SEM images of NVP-F after cycled at 5 C for 100 times.