Supporting Information

Room Temperature Single-Photon Emission and Lasing from All-Inorganic Colloidal Perovskite Quantum Dots

Xiaosheng Tanga, Zhiping Hua, Weiwei Chena, Xin Xingb, Wei Hua, Jing Qiua, Zhigang Zanga*, Juan Dub*, Yuxin Lengb,e, Xiaofang Jiangc, Liqiang Maid

- Key Laboratory of Optoelectronic Technology & Systems (Ministry of Education), Chongqing University, Chongqing 400044, China

- State Key Laboratory of High Field Laser Physics, Shanghai Institute of Optics and Fine Mechanics, Chinese Academy of Sciences, Shanghai 201800, China

- Institute of Polymer Optoelectronic Materials and Devices State Key Laboratory of Luminescent Materials and Devices, South China University of Technology, Guangzhou 510640, P. R. China

- Department of Materials Science & Engineering, Wuhan University of Technology

- School of Physical Science and Technology, Shanghai Tech University, Shanghai 201210, China

xstang@cqu.edu.cn, dujuan@mail.siom.ac.cn

Figure S1. The typical cubic crystal structure diagram of CsPbX3 represented by

CsPbBr3。

Figure S2. (a, c)TEM image of the CsPbCl3 and CsPb(Cl/Br)3 nanoparticles, the scale bar is 50 nm, the inset figure is the size distribution of nanoparticles. (b, d) HRTEM image of CsPbCl3 and CsPb(Cl/Br)3 nanoparticles, the scale bar is 5 nm.

Figure S3. The optical images of colloidal solutions in toluene under ultraviolet lamp,  the excitation is 365 nm.

Figure S4. The absorption spectra of CsPbX3 (X=Cl, Br and I).

Figure S5. Time-resolved PL decay curves obtained for CsPbX3 (X=Cl, Br) QDs, black (CsPbCl3), red (CsPb(Cl/Br)3), green (CsPbBr3).

Table S1. Time-resolved PL decays for CsPbX3 (X=Cl, Br) QDs, radiative recombination lifetimes (τr), nonradiative recombination lifetimes (τnr) and average decay lifetimes (τ).

|  | τr (ns) | τnr (ns) | τ (ns) |
| --- | --- | --- | --- |
| CsPbCl3 | 2.01 | 20.50 | 9.43 |
| CsPb(Cl/Br)3 | 3.33 | 36.25 | 21.33 |
| CsPbBr3 | 4.28 | 49.15 | 29.99 |

Figure S6. Scan scanning electron microscope (SEM) image of CsPbBr3 nanocrystal film, the scale bar is 1μm.

Figure S7. The comparison of the spectra of spontaneous emission (black) and amplified spontaneous emission (red) of CsPbCl3 QD in a normalized scale.

Table S2. The Q factors of CsPbX3 NCs.

| Wavelength (nm) | Q factor |
| --- | --- |
| 427 | 85.6 |
| 506 | 84.3 |
| 539 | 89.9 |