Supporting Information

Nickel-Iron Bimetallic Diselenides with Enhanced Kinetics for High-Capacity and Long-Life Magnesium Batteries

Limin Zhou, Fangyu Xiong, Shuangshuang Tan, Qinyou An*, Zhaoyang Wang, Wei Yang, Zhanliang Tao, Yan Yao*, Jun Chen, Liqiang Mai*

L. Zhou, F. Xiong, S. Tan, Prof. Q. An, Z. Wang, W. Yang, Prof. L. Mai

State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Hubei, Wuhan 430070, P. R. China

E-mail: anqinyou86@whut.edu.cn (Q. An); mlq518@whut.edu.cn (L. Mai)

Key Laboratory of Advanced Energy Materials Chemistry (Ministry of Education), College of Chemistry, Nankai University, Tianjin 300071, P. R. China

Prof. Y. Yao

Department of Electrical and Computer Engineering & Materials Science and Engineering Program, University of Houston, Houston, TX 77204, USA

E-mail: yyao4@uh.edu (Y. Yao)

Fig. S1. XRD pattern of the as-prepared precursor NiFe-LDH.

Fig. S2. SEM image of the precursor NiFe-LDH with corresponding phase mapping images (Ni, Fe, C, and O elements).

Fig. S3. Digital photos of the color change on Se powder and NaBH4 dispersed into deionized water .

Fig. S4. XRD patterns of the as-prepared NFS and NS (the right presents those of the two samples in enlarged range of 30-40o and 50-60o).

Fig. S5. Raman spectrum of the as-prepared NFS and NS.

Fig. S6. (a,b) SEM, (c) TEM, and (d) HRTEM images of the NS.

Fig. S7. Diagrammatic sketch of the potential change with time in GITT curve.

Fig. S8. (a) GITT curves and (b) calculated Mg2+ diffusion coefficient of the NS electrode.

Fig. S9. The magnification image of discharge GITT curve for the NS electrode between 25 and 40 mAh g-1.

Fig. S10. Nyquist plots of (a) NS and (b) NFS electrode at 30th cycle (SOD/SOC: state of discharge/charge).

Fig. S11. Cyclic voltammogram of the NS electrode at a scan rate of 0.5 mV s-1.

Fig. S12. (a) TEM images and (b) SAED patterns of the NFS electrode at various charge/discharge states. The marks (Ⅰ→Ⅳ) correspond to the marks in Fig. 4b.

Fig. S13. HAADF images of the NFS electrode at fully discharged state after 30 cycles.

Table S1. XRD refined structural parameters of the NFS.

| Atom | site | g | x | y | z |
| --- | --- | --- | --- | --- | --- |
| Ni | 4a | 0.75 | 0 | 0 | 0 |
| Fe | 4a | 0.25 | 0 | 0 | 0 |
| Se | 8c | 1 | 0.383 | 0.383 | 0.383 |

Space group: Pa-3 (No.205). Cell parameter: a=b=c=5.91490 Å. Rwp=1.82 %, Rp=1.40 %. g: occupancy. x, y, and z: atomic coordinates.

Table S2. Summary of electrochemical performance of different oxides and chalcogenides as cathode materials for magnesium batteries.

| Samples | Electrolyte | Initial capacity | Cycling stability | Ref. |
| --- | --- | --- | --- | --- |
| Mo6S8 | Mg(AlCl2BuEt)2/THF | 85 mAh g-1 at 0.2-0.3 mA cm-2 | ~100 mAh g-1 at 0.2-0.3 mA cm-2 | 1 |
| TiS2 | APC/tetraglyme | 250 mAh g-1 at 23.9 mA g-1 140 mAh g-1 at 47.8 mA g-1 | 115 mAh g-1 at 23.9 mA g-1 (40 cycles, 60℃) | 2 |
| Ti2S4 | APC/tetraglyme | ~190 mAh g-1 at 23 mA g-1 | 140 mAh g-1 at 23 mA g-1 (40 cycles, 60℃) | 3 |
| β-Cu2Se | Mg(AlCl2EtBu)2/THF | 120 mAh g-1 at 5 mA g-1 | ~100 mAh g-1 at 5 mA g-1 (35 cycles) | 4 |
| Sponge-like Mn3O4 | APC | ~190 mAh g-1 at 15.4 mA g-1 | ~100 mAh g-1 at 15.4 mA g-1 (20 cycles) | 5 |
| AC/Mo2.48VO9.93 | Mg(TFSI)2/AN | 114 mAh g-1 at 4 mA g-1 | ~235 mAh g-1 at 2 mA g-1 (15 cycles) | 6 |
| WSe2 nanowire | Mg(AlCl2EtBu)2/THF | ~220 mAh g-1 at 50 mA g-1 | ~203 mAh g-1 at 50 mA g-1 (160 cycles) | 7 |
| Peo2-MoS2 | APC | 75 mAh g-1 at 5 mA g-1 | ~70 mAh g-1 at 5 mA g-1 (30 cycles) | 8 |
| Flower-like CoS | Mg(AlCl2EtBu)2/THF | 120 mAh g-1 at 50 mA g-1 | 120.6 mAh g-1 (40 cycles), 105.9 mAh g-1 (60 cycles) at 50 mA g-1 | 9 |
| TiSe2 | Mg(AlCl2EtBu)2/THF | 130 mAh g-1 at 5 mA g-1 | ~90 mAh g-1 at 5 mA g-1 (50 cycles) | 10 |
| MoO2.8F0.2 | Mg(TFSI)2/PC | 40 mAh g-1 | ~75 mAh g-1 (18 cycles) | 11 |
| birnessite Mg0.15MnO2·0.9H2O/carbon cloth | Mg(TFSI)2/ diglyme | 145 mAh g-1 at 2 C | ~40 mAh g-1 at 2C (160 cycles) | 12 |
| Vanadium Oxide Nanoclusters | [Mg2(µ-Cl)2(DME)4][AlCl4]2 | 120 mAh g-1 at 320 mA g-1 | ~90 mAh g-1 at 320 mA g-1 (50 cycles) | 13 |
| NiSe2 | APC | 300 mAh g-1 at 20 mA g-1 | ~60 mAh g-1 at 20 mA g-1 (100 cycles) | This work |
| Ni-Fe bimetallic diselenide | APC | 320 mAh g-1 at 20 mA g-1 | ~150 mAh g-1 at 20 mA g-1 (100 cycles) | This work |

References:

[1]	D. Aurbach, Z. Lu, A. Schechter, Y. Gofer, H. Gizbar, R. Turgeman, Y. Cohen, M. Moshkovich, E. Levi, Nature, 407 (2000) 724-727.

[2]	X. Sun, P. Bonnick, L. F. Nazar, ACS Energy Lett. 1 (2016) 297-301.

[3]	X. Sun, P. Bonnick, V. Duffort, M. Liu, Z. Rong, K. A. Persson, G. Ceder, L. F. Nazar, Energy Environ. Sci. 9 (2016) 2273-2277.

[4]	Y. Tashiroa, K. Taniguchi, H. Miyasaka, Electrochim. Acta 210 (2016) 655-661.

[5]	L. Wang, K. Asheim, P. E. Vullum, A. M. Svensson, F. Vullum-Bruer, Chem. Mater. 28 (2016) 6459-6470.

[6]	W. Kaveevivitchai, A. J. Jacobson, Chem. Mater. 28 (2016) 4593-4601.

[7]	B. Liu, T. Luo, G. Mu, X. Wang, D. Chen, G. Shen, ACS Nano, 7 (2013) 8051-8058.

[8]	Y. Liang, H. D. Yoo, Y. Li, J. Shuai, H. A. Calderon, F. C. Robles Hernandez, L. C. Grabow, Y. Yao, Nano lett. 15 (2015) 2194-2202.

[9]	D. He, D. Wu, J. Gao, X. Wu, X. Zeng, W. Ding, J. Power Sources 294 (2015) 643-649.

[10]	Y. Gu, Y. Katsura, T. Yoshino, H. Takagi, K. Taniguchi, Sci. Rep. 5 (2015) 12486.

[11]	J. T. Incorvati, L. F. Wan, B. Key, D. Zhou, C. Liao, L. Fuoco, M. Holland, H. Wang, D. Prendergast, K. R. Poeppelmeier, J. T. Vaughey, Chem. Mater. 28 (2016) 17-20.

[12]	X. Sun, V. Duffort, B. L. Mehdi, N. D. Browning, L. F. Nazar, Chem. Mater. 28 (2016) 534-542.

[13]	Y. Cheng, Y. Shao, V. Raju, X. Ji, B. L. Mehdi, K. S. Han, M. H. Engelhard, G. Li, N. D. Browning, K. T. Mueller, J. Liu, Adv. Func. Mater. 26 (2016) 3446-3453.